Lecture 01 - Classification, Crystal Structures, Defects

Source: `STM/Material(1)/01_Classification_crystal_defects 2025-2026.pdf`

Purpose: open-note exam guide. It prioritizes answer structure, formulas, tutorial methods, and professor-style traps.

# Core Idea

Materials science links structure to properties. The professor's chain is: chemical bond and composition -> crystal/amorphous structure -> defects and microstructure -> mechanical, thermal, optical, electrical, technological performance. If asked to choose or explain a material, always connect class, bond, structure, and property.

# Material Classes and Bonding

Metals and alloys: metallic bonding with delocalized electrons. Consequences: good electrical and thermal conductivity, opacity/shine, high plasticity, high toughness, corrosion/oxidation issues, and preparation commonly by melting. Examples include Fe-C steel, Cu-Zn brass, Sn-Pb soldering alloys, Al-based light alloys.

Ceramics: compounds such as oxides, carbides, nitrides. Ionic/covalent or mixed bonds are strong and often directional. Consequences: high hardness, high melting point, good insulation, brittleness, difficult machining, usually produced by sintering rather than melting.

Glasses: oxide-based amorphous materials prepared by melting and quenching. They are hard and brittle, insulating, transparent, and soften progressively instead of melting sharply.

Polymers: organic macromolecules with covalent bonds along chains and weak secondary bonds between chains. Consequences: low density, easy processing, insulation, flexibility, low thermal/mechanical resistance.

Composites: matrix plus second phase/reinforcement. Classify by matrix (metal, polymer, ceramic, glass/glass-ceramic) or by reinforcement morphology (fibers, particles).

# Crystalline, Amorphous, Semi-Crystalline

Crystalline materials have atoms/ions/molecules in ordered positions in cells. Unit-cell parameters a, b, c and angles alpha, beta, gamma identify the structure.

Seven basic lattice systems plus centered variants form Bravais lattices. The lecture highlights FCC, BCC, and hexagonal compact structures. Examples: FCC Cu/Al/Ag/Au; BCC Fe/W/Cr; HC Mg/Ti/Zn.

Amorphous materials have only short-range order. Glasses and many polymers have no exact melting temperature; they soften progressively and are sometimes described as undercooled liquids.

Semi-crystalline materials include many polymers and glass-ceramics.

Allotropy/polymorphism means a crystalline solid changes crystal structure while still solid, with property changes in volume, thermal expansion, conductivity, E, density, etc. Fe, Ti, and SiO2 are examples.

# X-Ray and Miller Index Formula Box

Bragg law: n lambda = 2 d sin theta. n is an integer, lambda is wavelength, d is interplanar spacing, theta is the incident angle.

For cubic cells: d_hkl = a / sqrt(h2 + k2 + l2).

Miller indexes (h k l) identify crystal planes. XRD distinguishes crystalline from amorphous materials; broad peaks indicate smaller crystal size and amorphous material gives broad diffuse response.

# Point Defects

Point defects are atomic-size defects but perturb a region around them. They create local stress because atoms are not in their correct lattice positions.

Vacancies: empty lattice sites. They allow atomic motion from site to site, so they enable diffusion. Vacancy concentration increases with temperature by Arrhenius behavior: Nv/Ntot = C exp(-Ev/kT). At 0 K it would be zero, but absolute zero is unreachable.

Interstitial atoms: atoms crowded into interstitial positions, not lattice knots. Metallic lattices commonly accept H, C, N, O as interstitial impurities. Interstitial solid solutions have a solubility limit; beyond it a second phase forms.

Steel is the key example: C in Fe is an interstitial solid solution up to the solubility limit and improves mechanical properties by lattice distortion/internal stress.

Substitutional atoms occupy lattice knots and can be smaller or larger than host atoms, creating tensile or compressive local stress.

Hume-Rothery rules for substitutional solid solutions: similar atomic radius (difference below about 15%), same crystal structure, similar electronegativity, and compatible valence.

Ionic solids can have Frenkel defects (vacancy plus interstitial ion) and Schottky defects (paired cation and anion vacancies), increasing electrical conductivity.

# Dislocations and Plastic Deformation

Dislocations are line defects caused by lattice distortion. They are produced during solidification and plastic deformation and are normally present in commercial materials.

Edge dislocation: extra half-plane of atoms. Screw dislocation: spiral distortion around a dislocation line. Real dislocations are often mixed.

Plastic deformation in metals is possible because dislocations move. Perfect-crystal sliding would require breaking many bonds at once, giving a theoretical resistance far above real crystals.

Elastic deformation stretches bonds but does not move dislocations. Plastic deformation is irreversible because applied stress moves dislocations.

Work hardening: during plastic deformation, dislocations generate and accumulate. Their stress fields interact, block further motion, raise strength/yield stress, and reduce ductility.

Dislocations also interact with point defects, which is why alloys are stronger than pure metals.

Covalent solids and ionic solids are brittle because bond directionality or charge repulsion makes dislocation motion difficult. Metallic bonding is non-directional, so dislocations move smoothly and metals are ductile.

# Grain Boundaries and 3-D Defects

Monocrystals have all cells oriented the same way; polycrystals consist of grains, each with its own orientation, separated by grain boundaries.

Grain boundaries are surface defects, roughly a few atomic diameters thick, where crystalline order is disrupted.

Fine grain size generally increases mechanical strength. Grain boundaries also have high energy and can be more chemically reactive than grains.

3-D defects include precipitates/second phases when solubility limits are exceeded. Pores, cavities, and cracks are macroscopic defects that strongly reduce mechanical, electrical, and optical properties.

Strengthening methods in this lecture: substitutional solid solution, interstitial solid solution, grain size reduction, second phase/precipitates. The shared mechanism is lattice distortion and obstacles to dislocation motion.

# Amorphous Materials and Viscosity

Amorphous materials have local short-range order but no long-range periodicity. They are metastable and can crystallize if properly heated.

Glass viscosity decreases continuously with temperature, unlike crystalline materials with a sharp melting point.

Viscosity unit: 10 Poise = 1 Pa s. Example from the slides: water at room temperature has eta about 10^-3 Pa s, while silica at 1720 C has eta about 10^6 Pa s.

Transparency trap: glass and diamond can be transparent for different structural reasons; glass is amorphous with no long-range grain-boundary scattering, while diamond is crystalline but can be transparent because visible light does not have the right interaction with its bonding electrons.

# Closed-Question Traps

E and melting temperature follow bond strength; dislocation density controls plastic deformation and strength, not elastic modulus.

If an interstitial atom is added above solubility, the result is not "more interstitial solution only"; a second phase forms.

Crystalline does not mean defect-free. A perfect crystal is impossible at finite temperature because vacancies exist.

Polymers are not purely covalent solids in behavior: covalent bonds are along chains, weak secondary bonds are between chains.

Glass is amorphous and lacks a defined melting point, but it is formally treated as a ceramic sub-family in this course.

# Source Slide Checklist

This is a compact OCR/text extraction from the source PDF. Use it as a searchable reminder of the slide wording, not as a replacement for diagrams.

## Source page 1

GENERAL OVERVIEW AND

CLASSIFICATION OF MATERIALS,

CRYSTALLINE STRUCTURES,

DEFECTS

## Source page 2

The aim of this course:

• The aim of this course is to provide Mechanical and

Automotive Engineering students basic knowledge on

different classes of materials

• Relationship between structure of materials and their

properties (Materials Science)

• Structure of materials  chemical and physical

characteristics (e.g. chemical bonds,

composition, …)

• Materials Engineering

...

## Source page 3

MATERIALS OF INTEREST IN

ENGINEERING

• metals and alloys

• polymers

• glasses

• ceramics

• composites

(fuels, lubricants, paints, …....)

## Source page 4

The periodic table

METALS NON-METALS

“NOBLE”

GASES

## Source page 5

COV ALENT

WEAK

(e.g. Van

der Waals

PURE

METALS and

METAL

ALLOYS

Me + O

OXIDES

...

## Source page 6

OVERVIEW ON METALS AND

ALLOYS

• ELEMENTS (Fe, Ti, Al, Mg, Cu,…)

• Conductors for heat and electricity

• Prepared by melting

• Can be machined

• (almost) All are solid at room temp.

• Can form alloys

• Corrosion and oxidation issues

• Density ranging (typically) between 2,7 and 8 g/cm 3

## Source page 7

Pure metals and metal alloys consist of atoms and are characterized by

metallic bonding : the valence electrons of each atom, i.e. the electron

available for the bond, are delocalized and shared among all the atoms.

Most of the elements in the Periodic Table are metals.

Examples of metal alloys are:

- Cu-Zn (brass)

- Fe-C (steel)

- Sn-Pb (an alloy used for soldering)

Alloys are classified according to the majority element that is present in it.

The main classes of alloys are:

...

## Source page 8

Strong bond with non-localized electrons

Valence electrons forming an

electron cloud

Nuclei are

arranged in

an ordered

array

Each nucleus is bonded to the others by the global electric fi eld, but it is

NOT bonded to another specific nucleus.

Electrons are NOT bonded to a specific nucleus.

## Source page 9

Electrical and heat transfer properties

Ability of conducting electricity and heat due to the presen ce of mobile

electrons (electron cloud) inside metallic chemical bond

Properties of metals

Optical properties

No transparency to visible light due to the electron energy of the metallic

chemical bond (all visible radiations are absorbed); metal s are shine after

polishing

Mechanical properties

- High plasticity (rough definition: “high

...

## Source page 10

The bonding strength in metal bonds is quite variable

Bonding strength (BS) deeply affects:

- hardness (H)

-

melting point (MP)

Note: if BS ↑, then H and MP ↑

Examples:

- Ga melts at room temperature

- Hg is liquid at room temperature

- W is extremely hard and melts at a very high temperature (3430 °C)

## Source page 11

OVERVIEW ON CERAMICS

• Compounds (oxydes , carbides, nitrides, ..)(Al 2O3,

SiC, Si 3N4,…)( density ranging between 3 and 5 g/cm 3)

• hard and brittle, difficult to be machined

• Insulators

(heat and electricity)

• High melting point

• Prepared by

sintering or other processes, never

melting

...

## Source page 12

OVERVIEW ON GLASSES

• Prepared by melting of oxides

(SiO 2, Na 2O, CaO, Al 2O3, K 2O,...)

• Hard, brittle, can be deformed only at suitable

temperature, cannot be machined

• insulators (heat and electricity)

• Density of about 2,5 g/cm 3

• examples: window and car glasses, optical

fibers

## Source page 13

Reticular positions (= the

positions of atoms inside the

crystals) are occupied by

charged atoms ( IONS ) with

different size

Forces of ionic bond are due

to

attractive interactions

(Coulomb force) between

ions with opposite charge

...

## Source page 14

Coulomb bonding force Schematic representation of ionic bonding

in sodium chloride (NaCl)

IONIC

BONDING

ELECTRON

TRANSFER

● Crystal stability is assured by the

electrostatic interactions between ions of

opposite (+ or -) charge

●

...

## Source page 15

Properties of ionic solids

Optical properties

Some frequencies of visible light can interact with the elec trons involved in

the ionic bond and, accordingly, be absorbed; ionic solids c an be partially

transparent and coloured

Electrical properties

Ionic solids are good insulators; they can be conductors in aqueous solution.

Physical properties

- high melting points

due to the high

...

## Source page 16

He

-

Ne

-

Ar

-

Kr

-

Xe

-

...

## Source page 17

COVALENT BOND

is

HIGHLY DIRECTIONAL

Silica (SiO 2)

Note : the valence of one atom

can be roughly viewed as the

number of electrons available

for the bonds, and accordingly

as the number of bonds one

atom can form with other atoms.

## Source page 18

Properties of covalent solids

Optical properties

Transparent and colourless , as the bonding energy is higher than the

energy of visible light that so does not interact with the mat erial but passes

through it.

Electrical properties

Low electrical conducibility as electrons are strongly bon ded in specific

sites

Physical properties

- High melting point due to the high bonding strength

...

## Source page 19

OVERVIEW ON POLYMERS

• Organic macro-molecules,

natural or synthetic

• Prepared by organic synthesis

• Low density, less than

1 g/cm 3

• Easy to machine

• Insulators

(sound, heat and electricity)

• Low thermal and mechanical properties

...

## Source page 20

Polymers (e.g. nylon, polyethylene, polyvinylchloride, r ubber, etc.),

commonly referred to as “plastics”, basically consist of -C H 2-CH 2-CH 2-

molecular chains that have covalent bonding within each cha in (e.g., C-C

bond or C-H bond) and Van der Waals’ forces between the chains.

Due to the bonding, polymers are typically electrical and th ermal insulators.

However, conducting polymers can be obtained by doping, and conducting

polymer-matrix composites can be obtained by the use of conducting fillers.

• cannot sustain high temperature,

• show low mechanical resistance,

• are insulating to the passage of electricity,

...

## Source page 21

STRENGTH OF THE CHEMICAL BOND

MELTING TEMPERATURE

STIFFNESS

HARDNESS

THERMAL EXPANSION COEFFICIENT

Van der Waals Metallic Ionic Covalent

Comparison of some properties dependent on bond

## Source page 22

OVERVIEW ON COMPOSITES

• TWO PHASES :

MATRIX and SECOND PHASE

• Classified according to the matrix :

• Metal matrix composites

• Polymer matrix composites

• Ceramic matrix composites

• Glass and glass-ceramic matrix composites

• examples: wood, reinforced concrete, bones,…

## Source page 23

OVERVIEW ON COMPOSITES

• Can be classified according to the second

phase morphology :

• Fiber-reinforced composites (long fibers, short

fibers)

• Particle-reinforced composites

• The second phase can be: metal, polymer,

ceramic, glass

## Source page 24

STRUCTURE OF MATERIALS

## Source page 25

Argon (gas) Water (in gas state)

Silicate glass

(each Si atom is surrounded

by four O atoms)

Metals and ceramics

## Source page 26

From a structural viewpoint, solid materials can be divided into:

CRYSTALLINE

AMORPHOUS

SEMI-CRYSTALLINE

Metals, ceramics

Glasses,

polymers

Polymers, glass-ceramics

## Source page 27

CORRELATION STRUCTURE-

PROPERTIES

• …the aim of Materials Science

• CRYSTALLINE STRUCTURES

- Melting Temperature

• AMORPHOUS STRUCTURES

- They do not have a defined melting

temperature, but undergo progressive softening

## Source page 28

CRYSTALLINE STRUCTURE:

MELTING TEMPERATURE

• Melting temperature  Solid to liquid (T m)

• directly proportional to the material bond

strength

## Source page 29

MELTING TEMPERATURE

Tm

(°C)

Tm

(°C)

Tm

(°C)

W 3410 Mg 651 Al 2O3 2045

Ti 1675 Pb 270 SiO 2 1730

Fe 1536 Sn 232 MgO 2800

...

## Source page 30

Materiali per l’Ingegneria

M.Ferraris

## Source page 31

CRYSTALLINE STRUCTURE

• Chemical bond and crystalline structure:

atoms, ions or molecules in crystalline

structures are in ordered positions in

crystalline cells

• atoms, ions or molecules are at the equilibrium

distance between attraction and repulsion

forces:

bond length or bond distance

## Source page 32

CRYSTALLINE STRUCTURE

• “CRYSTALLINE materials: ordered positioning

of atoms (ex: metals ), or ions (ex: ceramics ) or

molecules (ex: polymers )”

• CRYSTALLINE

CELL

• a,b,c

0,1-0,26 nm

## Source page 33

CRYSTALLINE CELLS

a,b,c cell parameters

a,b,g cell angles

• identify the structure of crystalline materials by cell parameters

• a,b,c about 0,1-0,26 nm at room T and without ext. applied forces

a, b, c are the distance parameters

a, b, g are the angular parameters

From the unit cell… …to the entire crystal

Knots occupied by

atoms or ions

...

## Source page 34

CRYSTALLINE CELLS

• a,b,c change with T and applied forces

• At 0 K they are at the equilibrium distance

• When T increases, vibration around the

equilibrium distance cause

thermal expansion,

then melting .

## Source page 35

SEVERAL CRYSTALLINE CELLS

a = b = c a = b =  = 90° CUBIC

a = b  c a = b =  = 90° TETRAGONAL

a  b  c a = b =  = 90° ORTHORHOMBIC

a = b = c a = b =   90° ROMBOEDRIC

a = b  c a = b = 90° ,  = 120° HESAGONAL

a  b  c a = b = 90°   MONOCLINE

a  b  c a  b    90° TRICLINE

## Source page 36

There are 7 basic

lattice cells

Note:

a, b, c are typically within 0.1-0.29 nm

at T = 25 °C and without external

forces applied upon the crystal.

If T    vibrations of atoms/ions

around the knots

## Source page 37

Crystalline cells

## Source page 38

There are other 7 composed

lattice cells derived from the basic

ones.

These new 7 lattice cells may

have knots on some of their faces

(face-centred cells, FCC ) or

inside the cell ( body-centred

cell, BCC ).

All these 14 lattice cells are called

Bravais’s lattice cells .

## Source page 39

Face-centered cubic (FCC) cell

## Source page 40

Body-centered cubic (BCC) cell

## Source page 41

Hexagonal compact (HC) cell

## Source page 42

Es: Cu, Al, Ag, Au

Es: Fe, W, Cr

Es: Mg, Ti, Zn

BCC FCC

HC

## Source page 43

(h k l) are called Miller indexes

## Source page 44

Electromagnetic

radiation spectrum

E=h n

= c / n

E= energy

n = frequency

= wavelength

c=light speed

Energy, frequency

wavelength

...

## Source page 45

X-ray diffraction (XRD)

XRD of a crystalline

material (Au)

XRD of

amorphous silica

and crystalline silica (SiO 2)

## Source page 46

X ray diffraction

n  = 2 d sin q

(Bragg law)

n= number, 1, 2, 3…

## Source page 47

nλ = 2dsinθ

where n is an integer, λ is the wavelength of the

beam, d is the spacing between the diffracting planes,

and θ is the incident angle of the beam.

## Source page 48

X-ray diffraction of silicon carbide

(SiC)

Materiali per l’Ingegneria

M.Ferraris

## Source page 49

2 2 2l k h

adhkl

 

=

The interplanar distance d depends on:

- lattice parameters

- Miller indexes (h k l)

for a cubic cell (in this case a = b = c)

There are other (more complex) mathematical correlations for

the other types of crystalline cells.

## Source page 50

Assessment of

crystal size by

estimating the

broadness of the

diffraction peak:

a) 50 m

b) 1 m

c) 100 nm

d) 10 nm

e) 5 nm

...

## Source page 51

CRYSTALLINE STRUCTURE:

ALLOTROPHY and POLYMORPHISM

• A crystalline solid melts when heated

• Allotrophy or Polymorphism: change of

crystalline structure during heating (solid state

reaction)

• examples : Ti, Fe, SiO 2

• Allotrophy/Polymorphism  variation of

materials properties: (V, a, k, E, d,….)

## Source page 52

Examples

## Source page 53

CRYSTALLINE STRUCTURE:

DEFECTS

• Crystalline structure is not completely ordered

 LATTICE DEFECTS :

• ZERO-DIMENSIONAL DEFECTS

• MONODIMENSIONAL DEFECTS

• BIDIMENSIONAL DEFECTS

• THREE-DIMENSIONAL DEFECTS

## Source page 54

Lattice defects have influence on:

·

physical properties (e.g. density)

· mechanical properties (e.g. strength)

· technological properties (e.g. cold working ability,

electronic conductivity for semiconductors,

resistance to corrosion).

SOME PROPERTIES OF MATERIALS

(at the macro-scale )

CAN BE PROPERLY TAILORED BY

...

## Source page 55

Lattice defects of atomic dimensions (1 atom)

Actually, a part of crystal of about 100 atomic radii

around the defect is perturbed!

4 types of point defects:

• vacancies

• interstitial atoms

• substitutional atoms

• defects in ionic solids («couple»)

Zero-dimensional defects or point defects

## Source page 56

Vacancies Substitutional

impurities

Interstitial

atoms

Interstitial

impurities

ALL THESE LATTICE DEFECTS INDUCE HIGH PERTURBATION IN

THE CRYSTAL:

ATOMS AROUND THE POINT DEFECT(S) ARE MOVED AWAY

FROM THEIR EQUILIBRIUM POSITION, AND SO THERE IS A

...

## Source page 57

A lattice site (knot) is unfilled and it remains EMPTY

Vacancies allow atomic motion from a lattice site to another one (diffusion)

Sources of vacancies

• chemical impurities (e.g. ions with different charges (+) or (-))

• presence of one element with 2 different oxidation numbers

(valences) (e.g. iron, Fe: we can have Fe 2+ or Fe 3+)

• solidification processes (especially in metals)

• atomic vibrations induced by T

Vacancies

## Source page 58

Vacancies concentration depends on temperature according to Arrhenius’s law :

Nv = equilibrium number of vacancies

Ntot = total number of atomic sites

C = constant

Ev = energy required for the formation of a vacancy

K = Boltzmann’s constant

Metals at room T at equilibrium : Nv/N tot = 10 -17

 (1 vacancy every 100 million billion atoms)

Metals at high T (just below T melting ) at equilibrium : N v/N tot = 10 -4

 (1 vacancy every 10,000 atoms)

...

## Source page 59

An atom is crowded into an interstitial site (i.e., it does NOT occupy a LATTICE

KNOT ).

Atom from the crystal  self-interstitial (unusual)

Foreign atom  interstitial impurity atom.

Metallic lattices: common interstitial

impurity atoms are H, C, N, O.

Oxides (e.g. ceramics): small-size

metallic ions

solvent solute

Interstitial atoms

...

## Source page 60

In most cases, interstitial elements show atomic radius BIGGER than the

radius of the lattice holes.

The introduction of an interstitial atom causes perturbation and stress in

the crystal  the atoms around the interstitial atom are moved away

from their equilibrium positions (or lattice knots).

The crystal can accept only a limited amount of stress and distorsion .

Interstitial solid solutions cannot be obtained for every composition,

but there is a LIMIT OF SOLUBILITY of the interstitial atom in each

lattice  this is related to the maximum stress “accepted” by the crystal

## Source page 61

The positions of the Fe atoms are

SLIGHTLY DISPLACED

as C is added

Example : STEEL

(it can be viewed as a solid solution

of C in Fe)

Pure Fe lattice

STEEL

Fe atoms occupy the lattice knots

(equilibrium positions)

...

## Source page 62

The interstitial atom is added in an amount below

the limit of solubility  an interstitial SOLID

SOLUTION is formed

The interstitial atom is added in an amount above the

limit of solubility  an interstitial solid solution and a

second phase (with different crystalline structure and

composition) are formed.

Nature follows this way because of thermodynamics

reasons  a second phase presenting lower energy

(i.e. MORE STABLE) is obtained

## Source page 63

Substitutional atom is smaller or bigger than host atoms and occupies a lattice knot .

solute

solvent

solute

solvent

Substitutional atoms

Compressive stress Tensile stress

## Source page 64

Atoms of A and B can arrange in a random way or can form an ordered solid

solution

In general, two different classes of substitutional solid solutions can be

created:

A

B

An ordered structure will be destroyed at high temperature

because of thermal agitation

## Source page 65

Defects are caused by ionic couple with opposite charge .

Defects in ionic crystals

Frenkel defect :

One vacancy (cation or anion)

+

one interstitial ion

Examples of ionic solids are many ceramics

(e.g. alumina, Al 2O3, used as refractory material

in furnaces; zirconia, ZrO 2,…) and salts (e.g.

NaCl )

## Source page 66

Schottky defect :

anion vacancy

+

cation vacancy

Defects in ionic crystal

increase

electrical conductivity

## Source page 67

ARE POINT DEFECTS

«BAD THINGS»?

• ALLOYS and in general solid solutions are

possible because of interstitials and

substitutionals defects

• presence of substitutional impurities are

necessary for charge movement in

semiconductor science

….

## Source page 68

Materiali per l’Ingegneria

M.Ferraris

## Source page 69

Solid solutions: substitutional alloys

Atoms with similar radius (difference <15%), crystalline cell,

electronegativity and valence  substitutional solid solution

These are the four HUME-ROTHERY rules

## Source page 71

Solid solutions: interstitial alloys

- Atoms as interstitial defects different from those of

the main lattice

- Only small atoms can enter a metallic cell as

interstitial defects (max 10%)

- Ex.: carbon is an interstitial defect in the iron lattice

in steels, up to about 2%

- RFe = 1.24 Å, R C = 0.71 Å

## Source page 72

DISLOCATIONS can be seen as irregular lines on the cross-section of a

material at very high magnifications.

Dislocations caused distorsion

of the crystalline lattice around

a row of atoms .

Dislocations are produced:

• during solidification

• during plastic deformation

Dislocations are usually present

in commercial materials

...

## Source page 73

We can describe them by separating a dislocation into 2

different components:

· edge or linear

· screw

Real dislocations have both edge and

screw components, so they are

mixed dislocations

Real dislocations have a quite irregular and complex shape

## Source page 74

An extra half-plane is present in a region of the crystal

The DISLOCATION LINE of an edge dislocation (like that in the image) is a

vector perpendicular to the paper plane and pointing out of it.

Edge dislocations

## Source page 75

Dislocations in nature….!

• Dislocation: one lattice plane more….

Copper sulphide (CuS)

cactus!

## Source page 76

A screw dislocation does not include an extra plane: the plan es

perpendicular to the dislocation line show small distortio n and they trace a

spiral path around the dislocation line.

Dislocation line

Screw dislocations

## Source page 77

Materiali per l’Ingegneria

M.Ferraris

Dislocation motion

## Source page 78

Dislocation

motion

PLASTIC DEFORMATION

## Source page 79

Caterpillars

Caterpillar has a lot of legs; it cannot move them all togethe r, but it moves a

couple of legs at the same time.

Leg movement looks like a wave from the caterpillar’s hind le gs to its

forefeet.

Dislocations motion: simple analogies

NOT POSSIBLE!

OK!

## Source page 80

Motion of carpet fold

It is difficult to let slide a big carpet pulling it from the en d, because of the

friction with the floor; but if there is a fold (= the dislocation ) the carpet can

be moved by fold translation.

## Source page 81

Dislocations can move and accumulate

Dislocation movement makes easier the

PLASTIC DEFORMATION

(see the behaviour of metals…)

## Source page 82

Dislocation motion begins as yield strength has been reached 

PLASTIC DEFORMATION of a material is due to this phenomenon

Single crystal

Single crystal

Dislocations motion and plastic deformation

## Source page 83

Dislocation are particularly significant in PURE METALS

AND ALLOYS since they provide a mechanism for plastic

deformation , which is the cumulative effect of slip of many

dislocations .

Plastic deformation refers to IRREVERSIBLE

DEFORMATION or CHANGE IN SHAPE that occurs when

the force (stress) that cause it is removed. This is because

the applied stress causes dislocation motion that, in

turn, causes permanent deformation .

The plastic deformation is to be distinguished from elastic

...

## Source page 84

Perfect crystal deformation:

A lot of strong bonds are broken to

allow relative sliding of atomic planes

Resistance of a perfect cystal is

about 1000-10000 times higher than

that observed one in real crystals

(with defects)

Real crystal deformation:

Less amount of strong bonds are

broken when planes are sliding

...

## Source page 85

The movement of dislocations

generates new dislocations :

a dislocation “forest” is produced since the sample shows

PLASTIC DEFORMATION

There is repulsion between the stress fields around each

dislocation; therefore the average distance between

dislocations decreases and dislocations start blocking the

motion of each other

DISLOCATIONS ACCUMULATION

HIGHER RESISTANCE OF THE MATERIAL

...

## Source page 86

HARDENING is obtained during deformation of a metallic material by

increasing the number of dislocations .

Before deformation, the dislocation density is about 10 6 cm of dislocation

line per cubic centimeter of material. When a stress greater than the yield

strength is applied, dislocation begin to slip ( PLASTIC DEFORMATION

occurs).

Eventually, a dislocation moving on its slip plane can encou nter obstacles

that pin the ends of the dislocation line; as we continue to ap ply stress, the

dislocation can create additional dislocations.

The dislocation density can increase to about 10

...

## Source page 87

Perfect crystal

(0 dislocations/cm 3)

Very high

yield

strength

Real

polycrystalline

material

(10 6 cm/cm 3 )

Low yield

...

## Source page 88

+ - + - + - + - + - + - + - + - + - +

- + - + - + - + - + - + - + - + - + -

+ - + - + - + - + - + - + - + - + - +

- + - + - + - + - + - + - + - + - + -

+ - + - + - + - + - + - + - + - + - +

- + - + - + - + - + - + - + - + - + -

Two planes of the ionic crystal are slided into non-preffere d direction 

overlap of ions with equal charge  they reject to each other  CRYSTAL

FRACTURE .

Ionic solids

...

## Source page 89

In metals there is no repulsion due to the

presence of the delocalized electronic cloud !

## Source page 90

Covalent solids (e.g. diamond, SiC…):

 directional bonding is UNFAVORABLE to dislocation motion

COVALENT SOLIDS ARE BRITTLE MATERIALS!

Metallic solids:

 dislocation motion OCCURS SMOOTHLY (structures with dense

atomic packing, small lattice parameters, non-directiona l bonding) 

ductile materials .

METALS HAVE SIGNIFICANT PLASTIC DEFORMATION ABILITY

Remember that:

## Source page 91

Interaction between

dislocations and point

defects

Mechanical

hardening, cold

working

## Source page 92

INTERACTION between DISLOCATIONS

AND POINT DEFECTS

• DISLOCATIONS INTERACT with themselves (cold working,

hardening).

• Dislocations interact with point defects: dislocation motion is

slower in alloys than in pure metals

• Better mechanical properties of alloys vs pure metals

• Without dislocations, the plastic deformation of metals cannot

be explained

• Dislocations can be seen with Scanning or Transmission

...

## Source page 93

Cottrell «clouds»

## Source page 94

Preferential sliding planes for

dislocations

Low density plane High density plane

## Source page 95

Materiali per l’Ingegneria

M.Ferraris

Dislocations in CMSX-4 single crystal superalloy in the primary

creep range at temperature 950 °C and stress of 185 MPa. TEM

bright-field image (B. Dubiel AGH-UST)

Aleksandra Czyrska-Filemonowicz, International Centre of Electron Microscopy for Materials Science

& Faculty of Metals Engineering and Industrial Computer Science, AGH University of Science and

Technology, Krakow, Poland

## Source page 96

Materiali per l’Ingegneria

M.Ferraris

SOLIDIFICATION OF A LIQUID AND ITS STRUCTURE

1425 °C

or SiO 2

a 1730 °C

SLOW SPEED

SOLIDIFICATION

MONOCRYSTALLINE

STRUCTURE

...

## Source page 97

Materiali per l’Ingegneria

M.Ferraris

Nucleation and

growth,

formation of GB

in

polycrystalline

materials

## Source page 98

CRYSTALLINE STRUCTURE

• MONOCRYSTALS: crystalline cells all oriented

in the same way (ex. Si for microelectronics)

• POLYCRYSTALS: crystalline cells oriented in

the same way ONLY inside grains:

solidification too quick to allow same

orientation in entire lattice (ex .metals, alloys,

ceramics)

## Source page 99

Monocrystal (a) vs. polycrystal (b)

## Source page 100

Monocrystals

• Difficult to obtain compared to

polycrystalline materials

• Silicon for electronics

- Extra slow molten silicon solidification

(1-10 m per second)

- About 1.5 m length silicon cylinders

300 mm diameter, sliced as wafers

- About 10 defects/cm 2

## Source page 102

Materiali per

l’Ingegneria

M.Ferraris

## Source page 103

Polycristalline materials

• Natural solidification from a liquid metal gives a

polycrystalline metal

• Several grains, same cell orientation inside the

grain, grains separated by grain boundaries

Grains in

Al 2O3

Grains

in steel

## Source page 104

Most materials are polycrystalline and are made of many single crystals

Each small grain has a different crystallographic orientation respect to the others

Grains arise from material solidification

GRAIN BOUNDARIES separate grains: in a 3-D view they are SURFACES

Surface defects: grain boundaries

Grain boundaries:

area of about 2-5 atomic diameters,

where crystalline order does not

exist and the grains impinge on

each other when the solidification is

...

## Source page 105

 Grain size and orientation affect some material properties; for instance, finer grain

size, higher the mechanical strength of the material

 Grain boundaries have high energy state as they can be viewed as regions in which

dislocations accumulate (with their deformation energy); th erefore, grain boundaries

are more chemically reactive in conparison to grains

 Grain boundaries nucleate during solidification ; geometrical shape of each crystal

depends on restrictions due to adjacent grain growth.

 In most cases, grain size varies from 1 μm

to 1 cm (depending on the material, working

route etc.).

...

## Source page 106

GRAIN BOUNDARIES

• Observable by optical

microscopy after chemical

etching (e.g. by acids)

## Source page 107

Grain boundaries

and crack

propagation

## Source page 108

In this case, we will obtain an interstitial

solid solution and a second phase (i.e. a

PRECIPITATE with different crystalline

structure and composition)

Nature follows this way because of

thermodynamics criteria  the second

phase has lower energy (i.e. MORE

STABLE) is obtained

3-D defects

Part of the crystal is substituted by a different compound

...

## Source page 109

Pores and cavities can strongly decrease mechanical, electrical and

optical properties of materials

Cracks can strongly decrease mechanical properties leading to

CATASTROPHIC FAILURE (fracture ) of the material  this should

be taken in account particularly for ceramic-based materia ls ( in

Architecture especially rocks and stones, bricks, glass…)

Macroscopical defects (NOT lattice defects)

## Source page 110

Substitutional solid solution Interstitial solid solution

Grain size reduction Second phase

How to improve hardness and strength of materials?

We try to induce lattice distorsion

that creates stress fields in the lattice

opposing to plastic deformation

and dislocation motion

INCREASE IN

YIELD STRENGTH

## Source page 111

AMORPHOUS MATERIALS

• Disordered structure, no melting point

• glasses, polymers

• Short range order (few nm) (ex: Si 4+ and O --

ions are situated in tetrahedra in silicate

glasses

## Source page 112

• Local, short range order;

bond angle and length are

variable

• No order after few

nanometers

• “Undercooled liquids”

• Quick solidification of a liquid

• “No time to obtain a

crystalline structure” !

Amorphous silica

...

## Source page 113

Amorphous materials: silica glasses

Si 4+

O--

tetrahedron amorphous structure of silica:

tetrahedra chains

## Source page 114

Crystalline vs. amorphous silica (SiO 2)

## Source page 115

AMORPHOUS MATERIALS

• Amorphous materials are not

thermodynamically stable :

• They become crystalline if properly heated

• All liquids can be solidified quickly enough to

obtain amorphous solids

•

All liquids can be solidified slowly enough to obtain poly- or mono-crystalline solids

## Source page 116

• Ex: silica glass: bond angles, force and

length differ in different tetrahedra

• No melting temperature

• Viscosity vs temperature

•

The opposite than crystalline materials!

AMORPHOUS MATERIALS

## Source page 117

VISCOSITY

• Viscosity is a measure

of a fluid's resistance

to flow .

• It describes the internal

friction of a moving fluid

(e.g. tetrahedra chains in

a silica glass).

## Source page 118

VISCOSITY

• Viscosity Unit : Poise

10 Poise = 1 Pa∙s = 1 (N/m 2)∙s

• Example of viscosity:

H2O (room T) = 1 x 10 -3 Pa s

SiO 2(silica) (1720°) = 1 x 10 6 Pa s

## Source page 119

VISCOSITY: AMORPHOUS and

CRYSTALLINE materials

Viscosity decreases

continuosly for

amorphous materials.

This is not the case for

crystalline materials

Al 2O3

Glasses,

polymers

## Source page 120

VISCOSITY

annealing

softening

Working point

Melting point

## Source page 121

Materiali per l’Ingegneria

M.Ferraris

Viscosity curve of a glass

## Source page 122

Materion introduces zirconium-base

metallic glass alloys

February 19, 2014

/journal_content/56/10180/17353851/NEWS

Bulk metallic glasses are amorphous alloys

derived from unique alloy combinations

whose disparate atoms retain a random

structure when they solidify.

Amorphous alloys have unique properties,

including very high specific strength (often

...

## Source page 123

A couple of notes on optical properties…

single-crystal

Al 2O3

polycrystalline

Al 2O3

polycrystalline Al 2O3

with 5% porosity

Why glass and diamond gem are transparent?