Lecture 02 - Mechanical Properties Part 1

Source: `STM/Material(1)/02_Mechanical prop part 1 2025-2026.pdf; STM/Material(2)/Exercise1_text.pdf; Exercise2_solved_Ferraris.pdf`

Purpose: open-note exam guide. It prioritizes answer structure, formulas, tutorial methods, and professor-style traps.

# Core Idea

Mechanical properties are used for material selection and design. The first mechanical lecture builds the elastic/plastic language: stress, strain, Young modulus, Poisson ratio, yield strength, and how to read a tensile curve.

# Stress and Strain

Normal stress: sigma = F/A. In tensile/compression tests use initial area A0 unless the question asks true stress.

Engineering strain: e = (l - l0)/l0 = Delta l/l0. A strain of 0.002 is 0.2%.

Shear stress: tau = F/A0. Shear strain: gamma = tan theta.

The lecture also labels bending and torsion as stress states. For this exam, most calculations use axial stress/strain and simple sections.

# Elastic Behavior and Young Modulus

Hooke law: sigma = E e. E is Young modulus/elastic modulus, units MPa or GPa.

Elastic deformation is recovered immediately after unloading because bonds return to equilibrium length.

E is proportional to bond energy and melting temperature. Ranking: E_ceramics > E_metals >> E_polymers.

E is not related to dislocation motion. Low alloying in steels barely changes E; ordinary steel stays near 210 GPa.

Amorphous materials generally show lower E than comparable crystalline materials.

Composite E can be estimated by a volumetric mixture rule: Ec = E1 fv1 + E2 fv2 + ... when the loading geometry supports that approximation.

# Poisson Ratio and Elastic Design

Poisson coefficient: nu = - transverse strain / longitudinal strain. Transverse and longitudinal strains have opposite signs in uniaxial tension/compression.

Typical values: metals about 0.33; ceramics 0.17-0.27; polymers 0.33-0.5; always below 0.5.

If a cylinder in tension must reduce diameter by Delta d, compute transverse strain Delta d/d0, then longitudinal strain = - transverse strain / nu, then sigma = E e, then F = sigma A.

# Plastic Deformation and Yield

When stress is high enough and strain exceeds the proportional elastic region, Hooke law no longer applies. Some bonds break and reform in different positions; after unloading, only the elastic part is recovered.

Yield strength is the frontier between elastic and plastic behavior.

In steels, interstitial C pins dislocations. The upper yield point corresponds to first unpinning; the lower yield point is the lower stress needed after dislocations move more freely.

Some metals/alloys do not show a sharp yield point; then use the 0.2% offset yield strength.

# Tutorial Method: Elastic Tensile Calculations

Maximum safe load with safety factor: choose sigma_allowed = YS/n, compute area, then Fmax = sigma_allowed A. Exercise 2 example: Al cylinder d = 10 mm, YS = 150 MPa, n = 2 gives A = 78.5 mm2, sigma_allowed = 75 MPa, Fmax = 5890 N.

Required diameter for allowed elongation: e = Delta l/l0, sigma = E e, A = F/sigma, d = 2 sqrt(A/pi).

Comparing material elongation under same F, A, and l0: sigma is the same, e = sigma/E, so lower E gives larger elongation. The exercise compares steel, bronze, and polymer: the polymer elongates enormously because E is very low.

True fracture vs engineering fracture: engineering fracture uses initial area; true fracture uses final area at necking/rupture. If final diameter is one third of the initial diameter, final area is one ninth of initial area, so true fracture stress is much higher.

# Exam Traps

Do not mix MPa and Pa without converting. 1 N/mm2 = 1 MPa.

A 0.2% offset strain is 0.002, not 0.2.

If the question asks "without plastic deformation", compare to yield strength, not tensile strength.

Elastic modulus controls elastic elongation; yield strength controls onset of plastic deformation; tensile strength is the maximum engineering stress.

Alloying and heat treatment can change yield and tensile strength a lot but only slightly change E.

# Source Slide Checklist

This is a compact OCR/text extraction from the source PDF. Use it as a searchable reminder of the slide wording, not as a replacement for diagrams.

## Source page 1

MECHANICAL PROPERTIES

OF MATERIALS:

Fundamentals, elastic and plastic

behaviour

## Source page 2

Mechanical properties of

materials

• Materials choice

• Design issues

• Correlation requested properties/class of material

• Mechanical properties independent of time

• Mechanical properties dependent on time

• Mechanical properties dependent on temperature

## Source page 3

 (STRESS) and e (STRAIN ) : definition

 (STRESS) = F (force, Newton, N) / A (surface, m 2)

 = F/A ( N/m 2 = Pa) ( N/mm 2 = MPa )

DEFORMATION or STRAIN :

(dimensionless or %)

e = (l - l0)/l 0 = l/l 0

sample length = l

initial sample length = l 0

tensile stress, compressive stress, bending stress, shear stress

## Source page 4

Tensile and compression

stress/strain

A0

F

F

ll0

l0

F

F

l

A0

Tension Compression

Stress,  = F/A 0

Strain, e = (l - l0)/l 0

...

## Source page 5

Shear

A0

F

F

 (Shear stress),  = F/A 0

(Shear strain),  = tan 

## Source page 6

Torsion

T

T



Torsion  = T/A 0

Shear strain,  = tan 

Ao

## Source page 7

Stress-strain curves (tensile test)

• Standard tests!

gauge length, 2 in.

reduced section, 2.25 in.

diameter, 0.5 in.

diameter, 0.75 in.

radius 3/8 in.

ASTM (American Society for Testing and

Materials)

ISO

UNI EN

## Source page 8

Standard circular cross-section for tensile tests

Metallic

specimens

## Source page 9

For most of materials, low stresses correspond to

proportionally low deformations (direct

proportionality)

 = E e (Hooke law, E=Young modulus or

elastic modulus)

 = F/A

e = l/l o [E] = MPa or GPa

F/A = E l/l o

## Source page 10

Tensile test curve on a metal

Max. tensile strength

Elastic field

Plastic field

 = E e

## Source page 11

Elastic behaviour

• Small stress corresponds to small deformation

having a direct proportionality between them.

• Small deformations are immediately recovered

when stress is removed

• E =  / e = [N/mm 2] = [MPa]

Young’s modulus or Elastic Modulus E

(Hooke law)

## Source page 12

Elastic modulus and atomic bond

• E ceramics > E metals >> E polymers

• Elastic modulus is directly proportional to the

energy of the atomic bond (and melting

temperature)

• No fracture of bonds in the elastic field

• Increasing of the bond length when stress is

applied.

• Immediate recovering of the bond equilibrium

length after stress removal

## Source page 13

EQUILIBRIUM STATE

NO APPLIED LOAD

THE DISTANCE

BETWEEN ATOMS IS

THAT OF THE STABLE

CHEMICAL BOND

LOADING

(in the elastic

range)

DURING ELASTIC

DEFORMATION THE

BONDS BECOME

LONGER IN THE

DIRECTION OF LOAD

...

## Source page 14

Callister

How atomic

bonds are

responsible of

materials

properties

Condon-Morse curves

## Source page 15

Elastic modulus and bond strength

E is directly

proportional to

(dF/dr) ro

Strong bonds:

ceramics

Weak bonds: polymers

## Source page 16

Elastic modulus and melting

temperature

Material Temp

melting [° C]

E

(GPa)

TiC 3160 310

Al 2O3 2045 370

W 3410 393

Fe 1536 207

Cu 1083 111

Al 660 70

Pb 327 14

Polyetilene 130 1

...

## Source page 17

Diamond

WC

SiC

Al 2O3

TiC

Ni

Steel

CFRP**

Copper and its alloy

Ti and its alloy

Zn and its alloy

Al and its alloy

Mg and its alloy

GFRP

...

## Source page 18

More than 4 orders of magnitude between E of diamond and E of polymers!

SOLIDI COVALENTI

VETRI

Young’s modulus depends

on some parameters:

- Bonding energy

Stronger chemical bonds

 higher bonding energy

 higher E

- Amorphous vs.

crystalline structure

Amorphous materials show

lower E than crystalline

ones

...

## Source page 19

The elastic modulus E is assumed to be

(almost) independent of alloying

elements (e.g. interstitial atoms)  E =

210 GPa

Low amount of alloying elements 

the mean energy of the bond remains

constant  E = cost

High amount of alloying elements  E

= 190-230 GPa

THE ELASTIC MODULUS IS NOT

RELATED TO THE MOVEMENT

OF DISLOCATIONS!

## Source page 20

How to measure the elastic

modulus: from tensile curve

steel

Al

stress

strain

## Source page 21

How to measure the elastic

modulus

- Drawbacks of tensile tests :

Sample preparation

Destructive test

Unsuitable for brittle materials

• Measurement of the elastic

modulus by compression or

bending tests, indentations…

• Non destructive tests

## Source page 22

Elastic modulus by sonic test

• E= 0.9465 * (  2L4/t 2)

•  = costant depending on material shape

•  = sonic wave frequency;

• L= sample length;

•  = material density;

• t = sample thickness.

For photos and technical specifications pleas visit: www.imce.net/presentation

## Source page 25

Measuring elastic

modulus (E)

by

GrindoSonic

 Useful for highly

porous samples

 Very useful for quality

control!

 No limtiations on size

 Limitations on

geometry

## Source page 26

Elastic modulus vs T

W

steel Al

Elastic modulus, GPa

## Source page 27

Mixture rule : elastic modulus is a weighted average, based on the

volumetric fraction, of the elastic moduli of the components:

Ec = E 1·f v1 + E 2·f v2 + … E n·f vn

Composite with 50% vol. C fibres + 50% vol. polymeric matrix

Carbon fibers: E  200 GPa

Polymer: E  0.6 GPa

Composite E  (200*0.5+0.6*0.5)  100 GPa

Composite 30% vol. C fibres + 70% vol. polymeric matrix

Composite E (200*0.3 + 0.6*0.7)  60 GPa

ELASTIC MODULUS IN COMPOSITES

## Source page 28

Elastic modulus of a steel vs T

## Source page 29

lz/2

l0x

lx/2

l0z





z

y

z

x

eeee



 

 

...

## Source page 30

Non linear elastic behaviour

• Some polymers, cast iron, concrete,….

• E calculated locally

Strain

Stress

1

2

e1 e2

Secant modulus at 1 = 1/e1

Tangent modulus at 2 = d /d e

## Source page 31

Summary

Linear elastic

Behaviour

(most materials)

Non linear elastic

behaviour

(some polymers,

cast iron,

concrete,…)

Anelastic behaviour

Time is required to

recover deformation

after stress removal

(some polymers)

## Source page 32

Plastic deformation and chemical bond

• When applied stresses increases and corresponding

deformations are higher than about 0.002, the

Hooke law does not work any more.

• Bonds start breaking and, if possible , other bonds

are formed in different positions

• If the load is removed, the sample recovers only t he

elastic deformation, but a plastic, permanent

deformation is evident.

• The frontier between elastic and plastic deformati on is

defined yield strength or limit of proportionality

## Source page 33

ELASTIC

DEFORMATION

PLASTIC

DEFORMATION

BRITTLE

FRACTURE

(CLEA V AGE)

## Source page 34

e curve for metals

fracture

Tensile

strength

Upper

lower

y

strain

stress

necking

Elastic field Plastic field

Strain at fracture

Metals follow one

of the two curves

## Source page 35

In steel we have interstitial C,

causing the dislocations to pin (to

stop).

Thus, it becomes difficult for

dislocation to move and we need

higher load to make them to move

(upper yield point).

Then, the pinning will be gone and

dislocations can move freely and

we need smaller load to keep them

moving (plastic deformation going)

 lower yield point.

## Source page 36

Yield strength at 0.2 %

strain (0.002)

This type of monotonic

curve is observed, for

example, in pure metals,

FCC alloys, Al alloys.

## Source page 37

Yield strength for different

materials

 y [MPa]

steels 250 -1400

Ni alloys 200 -1600

Ti alloys 200 -1300

Cu alloys 60 -950

Al alloys 100 -650

Mg alloys 80 -300

Epoxy resins 30 -100

nylon 50 -90

poly stirene 35 -70

ABS 50

poly et hy lene 6-30

## Source page 38

Dislocations explain the

3 orders of magnitute

between theorethical

and experimental

yield strength

Without dislocations,

the yield strength would

be about E/8 (GPa)

Yield strength and dislocations

## Source page 39

Material Tensile Yield Stress (psi)

pure (99.45%) annealed Al 4 x 10 3

pure (99.45%) cold drawn Al 24 x 10 3

Al alloy - precipitated, hardened 50 x 10 3

a "perfect" single crystal of pure Al ca. 10 6

When you have slipping of crystalline planes in a real crystal (with

dislocation), a lower amount of chemical bonds will break compared to

a perfect crystal (without dislocations)  lower yield stress

Technological implications?

(1 MPa = 145 psi)

## Source page 41

Sliding plane

Shear stress

Dislocations provide an effective way for bonds to break and re-

form in another place, when load is applied.

Dislocation motion is favoured on

high density sliding planes

## Source page 42

Es: Cu, Al, Ag, Au

Es: Fe, W, Cr

Es: Mg, Ti, Zn

Hexagonal compact

BCC FCC

## Source page 43

• BCC e FCC have at least 12 sliding planes

• HCP has a maximum of 6 sliding planes

• FCC metals (Cu, Al, Ni, Ag, Au) and BCC (Fe)

are ductile, with large plastic deformation

• HCP metals (Ti, Zn) are more brittle

plane (111) for CFC,

with three sliding

directions <110>

## Source page 44

• Number of preferred slip

systems

- https://www.tec-

science.com/material-

science/ductility-of-

metals/influence-of-the-

lattice-structure-on-the-

ductility/

- FCC (Cu, Al, Ni, Ag, Au)

and BCC (Fe) metals

have large plastic

deformation

- HCP (Ti, Zn) metals

have smaller plastic

...

## Source page 45

BCC

FCC

## Source page 46

• Plastic deformation of grains in a stainless steel after lamination

from Callister

After deformation

## Source page 47

Stress-strain curve for Al

Max. tensile strength

## Source page 48

If we stop loading here a residual plastic deformation ( e res ) is still present

## Source page 49

Plastic (residual,

permanent)

deformation

## Source page 51

Metal specimens of steel

(left) and bronze (right)

before and after the test

NECKING :

reduction of the

resistant section

(lateral contraction)

due to a

rearrangements of the

material structure

## Source page 52

Ductile fracture

Necking Formation of pores

pore coalescence’

Propagation

Coarse surface due to

plastic deformation

Orientation 45°

## Source page 53

Tensile strength

behaviour for

different

materials

## Source page 54

Stress-strain curves for brittle

materials

ceramics, glasses;

brittle alloys, brittle

polymers (below Tg),

brittle composites

No (or limited) plastic

deformation

## Source page 55

Materiali per l’Ingegneria

M.Ferraris

Brittle fracture

• Without plastic deformation

- Flat fracture surfaces

- Along crystalline planes for mono-crystalline materials

(cleavage)

- Intergranular fracture for poly-crystalline materials

## Source page 56

Ductile and brittle fracture

surfaces

• Ductile fracture: plastic deformation at the crack

edge, slow crack propagation

• Brittle fracture: no plastic deformation at the cr ack

edge, quick crack propagation (catastrophic failure)

## Source page 57

Tensile strength ( ) and % e

deformation at fracture

• Material  (MPa) e (%)

• steel 400-2500 40-12

• Al alloys 300-770 8-16

• Al 2O3 sint. 200-340 negligible

• SiO 2 glass 110 negligible

• ZrO 2 sint. 80 negligible

• Polyesthers 40-80 1-2

• Nylon 70-160 50-200

• Epoxy 30-120 3-6

## Source page 58

How to modify plastic

properties of materials

• Make dislocation motion more difficult = increase

materials mechanical strength (and hardness)

• Grain size

• Solid solutions

• Precipitates and second phases

• Work hardening

• Perfect crystals/monocrystals

## Source page 59

grain boundary grain boundary

 y  0  kyd1 2

Hall-Petch law

d = grain diameter (avg)



y = yield strength

Materials related costant

Grain size can be modified by

thermal treatment

Grain size reduction

## Source page 60

Need for nucleating agents

(fine ceramic powders in the melt)

## Source page 62

Solid solutions

Dislocations motion slowed

Tensile stresses Compression stresses

• Metallic solid

solutions

(alloys) have

superior

mechanical

strength than

pure metals

## Source page 63

Materiali per l’Ingegneria

M.Ferraris

Role of alloying elements on

mechanical properties

## Source page 64

1 MPa = 145 psi; 20000

psi = 137.9 MPa

The efficacy in increasing the

yield strength is related to the

solute/solvent size ratio

## Source page 65

Second phases

## Source page 66

Orowan mechanism  ring dislocation around rigid inclusions

The efficacy of the mechanism is related to the number of particles

rather than the total mass of particles.

## Source page 67

Work hardening

Dislocation density: little-deformed

metals: 10 6 cm/cm 3 (10,000 m/cm 3);

highly-deformed metals: 10 12 cm/cm 3

(10,000,000 km/cm 3)

The material undergoes successive loading-unloading cylces (“cold working”)

 formation of new dislocations  accumulation of dislocations  barrier to further

deformation  strengthening of the material  increase of σy (and hardness).

## Source page 68

Ramberg-Osgood law

(plastic field):

σ = H×εn

H and n = constant

n is called work-hardening exponent

## Source page 69

COLD WORKING OF STEELS

Increase of σy

•REVERSIBLE PROCESS:

•COLD WORKING/ANNEALING

## Source page 70

Mechanism of multiplication

of dislocations («forest»)

Frank-Read mechanism

## Source page 71

(1)

(2)

(3)

(4)

(5)

(6)

## Source page 72

Work-hardening on metals and alloys

## Source page 73

1. Visualize different mechanism of hardening in stress-strain

curves:

metals/deformation-process-in-real-crystal-structures/

1. Visualize difference between Elastic deformation and

plastic deformation:

metals/deformation-process-in-real-crystal-structures/

metals/fundamentals-of-deformation/