Lecture 03 - Mechanical Properties Part 2

Source: `STM/Material(1)/03_Mechanical prop part 2 2025-2026.pdf; STM/Material(2)/Exercise3_text.pdf`

Purpose: open-note exam guide. It prioritizes answer structure, formulas, tutorial methods, and professor-style traps.

# Core Idea

This lecture adds test methods and failure modes: true/engineering curve, necking, compression and bending, creep, fatigue, fracture toughness, hardness, toughness, resilience, Charpy, and ductile-to-brittle transition.

# Tensile Curve Details

Engineering tensile curve uses original area and original length. After necking, engineering stress can drop even though local true stress in the neck continues to increase.

Necking sequence: localized plastic instability, pore formation, pore coalescence, crack propagation, fracture.

Ductility by elongation: A% = 100(lf - l0)/l0.

A standard ductile metal shows elastic region, yield, plastic region, tensile strength, necking, and fracture. Brittle materials fracture with little or no necking.

# Compression and Bending Tests

Compression is important for brittle construction materials such as brick, concrete, and ceramics. It can overestimate performance under real complex stresses because flaws are not opened as in tension.

Compression of ductile samples can show barreling.

Bending/flexural tests are often used for brittle materials. In bending, the top surface is in compression and the bottom surface is in tension; failure generally starts on the tensile side.

Three-point and four-point bending allow flexural strength calculation from failure load and specimen dimensions.

# Creep

Creep is plastic deformation under constant load even when the nominal stress is in the elastic field.

It is thermally activated: metals above about 0.3-0.4 Tm, ceramics above 0.6-0.7 Tm, amorphous materials above Tg.

Creep test: constant load, constant high temperature, record strain vs time.

Primary creep: elastic plus plastic deformation; strain rate decreases due to hardening.

Secondary creep: steady-state strain rate is low and almost constant because work hardening and annealing balance.

Tertiary creep: voids/microcracks form, cracks propagate, strain rate accelerates, rupture follows.

Higher stress and higher temperature shorten creep life. Large grains or single crystals improve creep resistance because there is less grain boundary sliding.

# Fatigue

Fatigue is failure under cyclic loading. It can occur below yield strength and below tensile strength, so it is dangerous even for ductile materials.

S-N/Wohler curve: stress S versus number of cycles N to failure. Use it to read fatigue life at a given stress or fatigue strength at a given life.

Stress amplitude: sigma_a = (sigma_max - sigma_min)/2.

Fatigue limit: below this stress, some materials do not fail within the considered cycle range. Fe, Ti, and steels can show a limit; Al and Cu alloys are treated differently and may fail after enough cycles.

Fatigue fracture surfaces show a smoother fatigue propagation region and a rough final catastrophic failure region.

Improve fatigue resistance by surface strengthening, coatings/environmental protection, better design to avoid notches, and fatigue/fracture mechanics life prediction.

# Fracture Mechanics

Macro-defects such as pores and cracks are stress concentrators. The local stress at the crack tip is higher than nominal stress.

Elliptical crack approximation: sigma_m = 2 sigma_0 sqrt(a/r_t). Larger cracks and sharper crack tips are worse.

Fracture toughness: KIc = Y sigma_c sqrt(pi a). It combines critical stress, crack size, and geometry. Failure occurs when applied K reaches KIc.

Ductile fracture has plastic deformation at the crack tip and slow/stable crack propagation. Brittle fracture has little plasticity and fast/catastrophic propagation.

Weibull/statistical scale effect: larger specimens have higher probability of containing a critical flaw, so they can fail at lower stress. Glass fibers can be much stronger than glass slabs because their volume/defect population is smaller.

# Hardness, Toughness, Resilience, Charpy

Hardness is resistance to localized compressive indentation. It can be measured with spherical or pyramidal indenters.

Brinell: HB = F/(pi D d). Vickers: HV = 1.854 F/L2. Rockwell measures penetration depth; values outside the scale range are not acceptable.

Hardness is useful because it is easier and less destructive than tensile testing. For steel, TS is roughly 3.45 HB.

Toughness is total energy absorbed up to fracture, the whole stress-strain area.

Resilience is elastic energy absorption. Ur = 1/2 sigma_y e_y = sigma_y2/(2E).

Charpy test measures absorbed impact energy of a notched sample. It is used to study ductile-to-brittle transition.

DBTT matters especially for BCC metals such as Fe at low temperature. FCC metals such as Cu and Ni are generally more ductile over temperature.

# Tutorial Method: Creep and Fatigue Questions

If asked to draw creep curves for different temperatures or stresses, keep the same three stages but shift higher T or higher stress to larger strain and shorter rupture time.

If asked about microstructure in creep: monocrystalline or large-grain materials resist creep better than fine-grained polycrystals because grain-boundary sliding is reduced.

If asked to use fatigue curves: compute stress from load and area first, then read N from the S-N curve. With a safety coefficient, reduce allowable stress or increase required diameter accordingly.

# Source Slide Checklist

This is a compact OCR/text extraction from the source PDF. Use it as a searchable reminder of the slide wording, not as a replacement for diagrams.

## Source page 1

MECHANICAL PROPERTIES

OF MATERIALS:

Additional details and testing

methods

## Source page 2

“True” engineering curve

necking Formation of pores

Pores coalescence

Crack propagation

## Source page 6

Metallic samples

for tensile test

U4G5kcpcM

Excellent video on

tensile test

## Source page 7

Steel Pure metals

a) Au and Pb at RT (100% necking), metals and polymer

at high T

b) Standard ductility

c) Brittle fracture (no necking)

## Source page 8

Yield strength

(ss, sy, s0,2 )

(ss, sP(0,2) )

Yield strength or proportional

limit (R p0,2 )

Yield Strength (YS, S y),

“Yield Strength (offset = 0.2 %)”

## Source page 9

Upper and lower yield

strength

Upper Yield Strength (UYS)

and Lower Yield Strength

(LYS)

In steel we have the solute (Carbon atoms) in Fe as interstitials.

They cause the dislocations to pin. So it becomes difficult for

dislocation to move and we need higher load to make them move

(upper yield point). Then at some point the pinning is gone and

dislocations can move freely and we need smaller load to keep

them moving (plastic deformation going) and that would be the

lower yield point.

...

## Source page 10

(sMAX )

(R m)

Tensile Strength (TS, S u, UTS)

## Source page 11

elongation %

(A t)

Maximum elongation (Elmax)

0 

l

l l

Ductility

## Source page 12

Typical stress-strain curves

failure

tensile strength

upper yield point

lower yield point

sy

strain

stress

sample ‘necking’

elastic

region

plastic

...

## Source page 14

It is adopted for measuring the strength of materials used in compression

(the majority of structural materials for Architecture: br ick, concrete…) and

for calculating the forces required in manufacturing processing

It is useful for brittle material : pre-existing micro- or macro-defects are not

enlarged  higher strength and strain than in tensile test. However, th is test

overestimates the material resistance: the component can r each premature

failure (in comparison to compression data) under real oper ating conditions

if complex stresses (e.g. compression + torsion + bending) are present.

Effect of

tensile test

on flaws

Effect of

...

## Source page 15

Tension Tension

Compression

Same material!

## Source page 16

Warning!

company/library/test-

types/compression-test

«barrelling»

## Source page 17

COMPRESSION TEST

## Source page 18

Bending or flexural test

## Source page 19

It is often used for measuring

the strength of

brittle

materials .

There are compressive stress

on the top surface and tensile

forces on the bottom surface .

The results of the bending test

are similar to the stress-strain

curves obtained by tension

test;

the maximum stress at

...

## Source page 20

3-point or

4-point bending test

Block of concrete

Highly crystalline polymer

## Source page 21

Asymmetric 4 point bending for ceramic joined

materials

F

le

Fe FeFiFi

F

li

Mf

T

T = F le - li

le + l i

## Source page 22

BENDING TEST on Al 2O3

and glass

s (MPa)

e

BENDING TEST on materials

with plastic deformation

## Source page 23

Flexural strength of ceramics

## Source page 24

Condition of use!! T ????

## Source page 25

TEST:

• Draw e versus t (strain vs time) when a material is

loaded at s = constant, in the elastic field, in two

conditions:

• Room temperature

• High temperature (e.g. 50% Tm)

## Source page 26

TEST

• Draw e versus t (strain vs time) when a material is

loaded at s = constant, in the elastic field

## Source page 27

TEST

• Draw e versus t (strain vs time) when a material is

loaded at s = constant, in the elastic field

## Source page 28

CREEP

Plastic deformation even if stress is in the elastic

field

fracture

Elastic deformation

Creep I

Creep III

Creep II

## Source page 29

Materiali per l’Ingegneria

M.Ferraris

CREEP

Constant load in the elastic field can g ive to a

plastic deformation, progressive to fracture.

•Thermally activated process

Metals T>0,3-0,4 T

melting

Ceramics T> 0,6-0,7 T melting

Amorphous materials T>T glass

creep test

: a constant load is applied at a

...

## Source page 30

Creep test execution: a specimen is subjected to a

constant load and strain is measured during a

significant period of time while maintaining the

temperature high and constant .

CONSTANT TEMPERATURE

(FURNACE)

SAMPLE

LOAD

(CONSTANT WEIGHT)

## Source page 31

Tertiary creep: at grain boundaries some

microcracks and voids are formed 

weakness points  cracks propagation 

material rupture

Primary creep:

we have elastic + plastic deformation;

the latter is favoured by dislocation

movement. The deformation rate

(dε/dt) progressively decreases.

Secondary creep:

the deformation rate (dε/dt) is low in

comparison to that of primary creep

...

## Source page 32

(c)2003 Brooks/Cole, a division of Thomson Learning, Inc. Thomson Learning ™ is a trademark used herein under

license.

Dislocations can climb (a) when atoms leave the dislocation line to create

interstitials or to fill vacancies or (b) when atoms are attached to the

dislocation line by creating vacancies or eliminating interstitials

Stage I: primary creep

## Source page 33

Stage II : steady state

nCRn

ss AT R

ECdt

d

 

e

e  









...

## Source page 34

Stage III: tertiary creep

## Source page 36

strain

tIME

increasing

load

Effect of the applied load

## Source page 37

increasing

temperature

strain

tIME

Effect of the working temperature

## Source page 38

°C

Experimental creep curves for a borosilicate glass

at 200 and 420 °C, from 18 to 36 MPa)

## Source page 39

How to increase creep resistance?

• High melting T and E materials

• Large grains or mono-crystals (small grains

increase grain motion at the grain boundaries)

• Solid solutions (to restrict dislocation glide)

• Precipitates (to restrict dislocation glide)

• Second phases (composites) (to restrict

dislocation glide)

Effect of grain size on yield strength???

## Source page 40

Scienza e Tecnologia dei Materiali

M.Ferraris

Grain size effect on creep

dg (average grain

diameter= 170 microns

Time (hours)

Creep tests at 1000 °C,

10 hours, 17MPa

## Source page 41

Scienza e Tecnologia dei Materiali

M.Ferraris

Crystalline structure effect on creep

-large grains can increase creep resistance because there is less grain boundary surface able to slide; several small

grains slide one on the other one; with a few large grains this is less evident;

-even longer creep life if you have a single crystal with no grains at all

## Source page 42

TEST:

• Apply a tensile stress to a material in the elasti c

field.

• Can this material fail?

• Repeat the test several times.

• Is it possible to have the material failure ?

• If yes, draw a graph with the applied stress

(s) versus the number of cycles (N)

necessary to achieve the material failure

## Source page 43

S-N curves: stress (S) vs number of cycles

(N) to obtain failure

N

S Fe, Ti, steels

Al, Cu

Dispersion range due

to experimental

measurement of fatigue

Fatigue limit

Wohler curves

## Source page 44

Fatigue

• Failure of materials due to cyclic loading.

• Main reason of mechanical failure of materials

• Failure happens at stress lower than sR or sY

• Catastrophic failure of materials (ALSO FOR DUCTILE

MATERIALS !)

• Fatigue tests: materials are cyclically loaded at different

stresses up to failure.

• Fatigue limit: when cyclically loaded below this limit,

materials do not fail (time considered by the graph)

## Source page 45

Experimental measurement: fatigue testing

Rotating-bending test: the specimen is rotated and a load perpendicular to

the rotational axis is imposed.

This test is very time-consuming  the specimens are tested under several

millions of stress cycles!

## Source page 46

S-N curve

s a s max s min

S=

N

S smax , smin : applied

stresses during tests

Fracture zone

Safe zone

Fatigue limit

## Source page 47

Materials and Fatigue

• Between 35-65% of their tensile strength most of

metals fail because of fatigue (e.g. Fe, Ti alloys,

intrinsical fatigue limit)

• Other metals fail in any case after a given limit (e.g. A l,

no intrinsical fatigue limit)

• Fatigue resistance: stress necessary to fracture the

material after a given number of cycles at this stress

• Fatigue life: number of cycles necessary to fracture

the materials at a given load .

## Source page 48

Materiali per l’Ingegneria

M.Ferraris

A 78.5 mm2

Stress amplitude 127MPa

A cylindrical component (10 mm diameter) is cyclically loaded at

10 kN (compression, tensile stresses). Calculate its fatigue life if

the component is made of brass, aluminum alloy or steel

## Source page 49

Fatigue: fracture surface

Starting point (macroscopic surface

defect)

Starting

point

Fatigue surface

(smooth)

Catastrophic failure,

rough surface

## Source page 50

Fatigue: fracture surface

Fatigue surface, smooth

Catastrophic brittle failure,

also on ductile materials,

rough surface

## Source page 51

Ductile and brittle fracture

• Ductile fracture: high plastic deformation at the

crack tip, slow crack propagation (i.e. stable

propagation)

• Brittle fracture: no (or low) plastic deformation at t he

crack tip, quick crack propagation (i.e. unstable

propagation), catastrophic failure

## Source page 52

Static loads Cyclic loads

Intrusion bands

## Source page 53

Stress intensity factor

• Macro-defects (pores, cracks) in

all materials act as stress

concentration factors

• True stress on the material at the

tip of the crack (s m) is higher than

the nominal stress (

s

0)

rt = radius of the crack

a = length of a crack on the

surface

...

## Source page 54

Stress intensity factor for elliptical cracks with

length = 2a and small curvature radius:

s m  2s 0

a rt









1 2

Callister

s0= nominal stress

sm= stress on material

...

## Source page 55

Materiali per l’Ingegneria

M.Ferraris

Crack propagation

Role of : rt = radius of the crack

a = length of a crack on the material surface

- If plastic deformation is possible,

rt can increase 

decrease of

sm

- If plastic deformation is not possible  catastrophic failure.

- Griffith Theory (with subsequent Irwin modifications)

quantifies these issues

...

## Source page 56

KIc = Y sc (p a) 1/2 (MPa m 1/2 )

Fracture thoughness

(mode I)

a = half length of the crack

Y = geometrical parameter

Crack propagation and critical parameters

sc = critical stress, crack propagation

for s > sc

## Source page 58

KIC critical

parameters

(defect length and

stress)

above which there is

failure ( all materials )

KIc = Y sc (p a) 1/2

(ASTM E 399)

PS-ZrO 2 8-12

## Source page 59

Materials

## Source page 60

The strength of materials (for allowing crack propagation) is given

by the combination of:

- fracture tiughness

- crack size

- sample geometry

## Source page 61

WEIBULL STATISTICS

The PROBABILITY of fracture is linked to the

dimensional distribution of the defects in the material

volume and to the probability of finding cracks of

certain dimensions in a sample

Larger samples statistically fail under lower loads 

greater probability of containing defects of critical size

SCALE EFFECT!

## Source page 62

Mechanical strength - «chain analogy»

The resistance of a chain depends on the

weakest element

If the resistance of each element is

randomly distributed and the probability

of NOT BREAKING of a chain of length

L is P s (L) then the probability of not

breaking of a chain of length 2L will be:

Ps(2L) = Ps(L)·P s(L)

Note on the scale effect (see previous slide):

as P

s(L) ranges between 0 and 1, then Ps(2L) < Ps(L))

## Source page 63

Example: glass fibres

 Tensile strength of a glass

slab around 100 MPa

 For glass fibres  900-1000

MPa

 Scale or volume effect 

Weibull statistics

 Tensile strength can reach

values comparable to the

compressive strength

## Source page 64

Materiali per l’Ingegneria

M.Ferraris

## Source page 65

How to increase materials fatigue

resistance?

• Surface strengthening

methods

• Environment (corrosion?) 

coatings

• Suitable mechanical design

• Fatigue and fracture

mechanics to model and

predict components life !

Strengthened surface

Normal surface

## Source page 66

Notches in engineering components

How to solve?

## Source page 67

Finite Element Analysis (FEA)

## Source page 68

Examples of different r

and stress concentration

by Finite Element

Analysis (FEA)

## Source page 71

It is a measure of the material resistance to localized compressive

stress due to INDENTATION .

The indenter is subjected to a load and causes a localized ela stic

deformation, followed by a plastic deformation which leads to an

indentation (imprint ).

Resulting indentations are observed and measured.

Different scales of hardness exist; the hardness

H can be expressed

as F/A , where A is the area of the indentation (note that H is formally

expressed in GPa ), or as the depth of the indentation (H is

expressed in μm or mm ).

Shape of the indenter:

...

## Source page 72

Basis

Loads

(changeable weights)

Head of the machine

Lever for load application

Sample holder

Indenter

Sample

Handwheel

Test execution

## Source page 73

Brinell test : spherical indenter

HB = F/( pDd) = load/indentation area

Vickers test: pyramidal indenter

HV = 1.854(F/L 2), where L is the imprint diagonal length

Indenter

Sample

surface

Indenter is above

sample surface

Indenter is subjected to a

load and it penetrates

into sample surface

...

## Source page 74

Vickers

Brinell

## Source page 75

Rockwell Hardness

measures penetration depth

## Source page 76

example: 60 HR30W = superficial Rockwell hardness =

You measure 60 on a scale 30W, with a Rockwell hardness test

## Source page 77

Example: 80 HRB= Rockwell hardness = 80 scale B

Values lower than 20 or higher than 100 are not acceptable

## Source page 78

Correlation hardness/tensile properties

Steel TS: about= 3.45 HB

brass

Cast iron

steel

78 HB

σmax

This correlation is useful because

hardness test is easier to be

performed than tensile test and it does

not fracture the sample.

This is the reason why the

...

## Source page 80

Vickers micro-hardness

on a brittle material

Quality of

joining

## Source page 81

AGAIN……..

## Source page 82

Materiali per l’Ingegneria

M.Ferraris

Toughness and resilience

• Toughness = energy absorbed up to fracture = area of se curve up

to fracture ) (J / m 3 )

• Resilience = energy absorbed under mech. impact (notched samples)

Stress

strain

Brittle, low ∫ s de

Ductile, tough, plastic…..large ∫ s de

## Source page 83

Stress

Fracture elastic energy or resilience modulus (U r)

Ur = ∫ s de( between e0 and

ey) (ELASTIC FIELD )

s = E e e ysy / E

Ur = ½ sy ey  ½ sy

2 /E

strain

## Source page 84

Charpy test :

Assessment of the

resiliency  energy

necessary to

fracture a notched

sample

(impact of a

hammer)

Starting position

hammer

scale

final position

...

## Source page 85

Absorbed impact energy vs. temperature for several steels: ductile to

brittle transition

Absorbed impact energy

Role of C and Fe 3C on dislocation motion and ductile to brittle transition

## Source page 86

Materiali per l’Ingegneria

M.Ferraris

Effect of ductile to brittle transition...

• 4 °C

• steel

## Source page 87

Importance of Brittle to Ductile Transition Temperature

The Titanic

P/S too High !

Mn too low !

Courtesy of L.L.Snead, ORNL, USA

## Source page 88

Work of : Leihly, Braamfitt, and Lawrence. Practical Failure Analysis 1(2) 2001.

Importance of “Ductility ” for Engineering Materials

Ductile-to-brittle

transition temperature

5 0

1 0 0

1 5 0

2 0 0

2 5 0

3 0 0

3 5 0

-1 0 0 -5 0 0 5 0 1 0 0 1 5 0 2 0 0

...

## Source page 89

Importance of Brittle to Ductile Transition Temperature

120 °C Test, Ductile -32 °C Test, Brittle

Titanic Hull Plate

Courtesy of L.L.Snead, ORNL, USA

## Source page 90

Fracture surfaces after Charpy test (V-

notched) at given T

Ductile to brittle transition

## Source page 91

• Increasing temperature...

-- increases % EL and KIC

• Ductile-to-Brittle Transition Temperature (DBTT) ...

D  B transition temperature

BCC metals (e.g., iron at T < 914°C)

Impact Energy

Temperature

High strength materials ( sy > E/150)

polymers

More Ductile Brittle

Ductile-to-brittle

transition temperature

...

## Source page 92

Ex: Cu, Al, Ag, Au

Ex: Fe, W, Cr

Ex: Mg, Ti, Zn

HEXAGONAL

BCC FCC

## Source page 93

Materiali per l’Ingegneria

M.Ferraris

- https://www.tec-

science.com/material-

science/ductility-of-

metals/influence-of-the-

lattice-structure-on-the-

ductility/

(Cu, Al, Ni, Ag, Au)

(Fe)

## Source page 94

CHARPY tests on

steel at different T:

at room T

2.22 J/mm 2

at -200 °C

0.04 J/mm 2

CHARPY test on steels

with same composition

but different thermal

treatments:

C40 steel annealed

0.89 J/mm 2

...

## Source page 95

DUCTILITY TEST

o

o f

STRAIN

l

l l) ( 100%  o

o

necking

A

A Af ) ( 100%



## Source page 96

Materiali per l’Ingegneria

M.Ferraris

## Source page 97

T1

T2

T3

T4

T1<T2<T3<T4

Effect of T

## Source page 98

Stress/strain curves vs Temperature

Fe Polymers (PMMA)