Lecture 04 - Thermal Properties

Source: `STM/Material(1)/04_thermal properties_2025-2026.pdf; STM/Material(2)/Exercise4_Q_solved_Ferraris.pdf`

Purpose: open-note exam guide. It prioritizes answer structure, formulas, tutorial methods, and professor-style traps.

# Core Idea

Thermal properties describe how a material responds to heat: temperature rise, dimensional change, energy transport, melting/softening, and thermal stresses. The exam simulation specifically asks heat conduction mechanisms, k ranking, diamond, and thermal expansion/stress calculations.

# Heat Capacity and Specific Heat

Heat capacity C is the ratio between heat added and temperature increase: C = dQ/dT or DeltaE/DeltaT, units J/K.

Specific heat c is heat capacity per unit mass: c = dQ/(m dT), units J/(kg K). cp is at constant pressure, cv at constant volume; at room temperature the difference is small for many solids.

Atomic/molecular heat is per mole and is often about 25 J/(mol K) for many solid elements at sufficiently high temperature.

During phase transformations, heat can be spent on the transformation without increasing temperature.

# Thermal Conductivity

Thermal conductivity is the ability to transfer thermal energy from a hotter region to a colder region.

Formula for 1-D conduction: Q_energy = k A t DeltaT / Delta x. Heat flux q = k DeltaT / Delta x.

k has units W/(m K). A is area, t is time, Delta x is thickness, DeltaT is temperature difference.

Mechanisms: free electrons and phonons. k_total = k_lattice + k_electrons.

Metals: free-electron contribution dominates, so k is high and related to electrical conductivity.

Ceramics: phonon contribution dominates; usually lower k than metals.

Glasses: lower k than crystalline ceramics because vibrational waves propagate poorly without long-range order.

Polymers: very low k because heat is dissipated by vibration/rotation of molecular chains; amorphous polymers are especially low.

Porous materials have low k because air in pores is a poor heat conductor. Foams and aerogels exploit this.

# Useful k Values and Ranking

Exercise values: Cu 398 W/mK, Al 247, Fe 81, steel 52, stainless steel 16.

Ceramics/glasses examples: MgO 38, Al2O3 30, MgAl2O4 15, SiO2 glass about 2, soda-lime glass about 1.7.

Polymers examples: polyethylene 0.4, nylon 0.24, PTFE 0.25.

Ranking to state in theory answers: k_metals > k_ceramics >> k_polymers, with glasses below crystalline ceramics.

Diamond has very high k because of strong bonds, high E, low defects, similar atomic masses, and simple crystalline cell.

# Thermal Expansion

On heating, atoms vibrate more and average bond distance increases, so solids expand.

Thermal strain: e_th = DeltaL/L0 = alpha DeltaT.

Linear expansion: DeltaL = alpha DeltaT L0.

alpha units: K^-1 or C^-1. It varies somewhat with temperature.

Typical ranges from slides/exercise: polymers about 50-400 x 10^-6 K^-1 (exercise simplified 100 x 10^-6 K^-1), metals about 5-25 or 15-30 x 10^-6 K^-1, glasses about 0.5-20 x 10^-6 K^-1, ceramics about 0.5-15 or 3-7 x 10^-6 K^-1.

Strong bonds give high E, high melting temperature, and low thermal expansion coefficient.

# Thermal Stress and Thermal Shock

If a body is free, it expands or contracts and stress may remain low.

If expansion/contraction is constrained, thermal stress develops: |sigma| = E alpha |DeltaT|.

Heating a constrained rod wants to elongate, so the constraint produces compression. Cooling a constrained rod wants to contract, so the constraint produces tension.

Joined materials with different CTE develop residual stresses during cooling. If alpha_B > alpha_A, material A is in compression after cooling; if alpha_B < alpha_A, material A is in tension.

Thermal shock resistance first approximation: TSR about sigma_f k / (E alpha). High k and low alpha are favorable; high strength helps; brittle materials often fracture under thermal stresses.

# Tutorial Methods

Conducted energy: convert thickness to meters, area to m2, time to seconds, then Q = k A t DeltaT / Delta x.

Example from Exercise 4: polymer component, k = 0.58 W/mK, DeltaT = 30 K, Delta x = 0.002 m, A = 1 mm2 = 1e-6 m2, t = 3600 s. Heat flux = 8700 W/m2, energy = 31.32 J.

Expansion example: steel alpha = 14 x 10^-6 C^-1, L0 = 50 m, DeltaT = 30 C. DeltaL = 14e-6 x 30 x 50000 mm = 21 mm.

Constrained stress example: steel E = 207 GPa, alpha = 12e-6 C^-1, DeltaT = 60 C. sigma = 207000 MPa x 12e-6 x 60 = 149 MPa compression.

Temperature limit example: with constrained brass, sigma = E alpha DeltaT; solve DeltaT = sigma/(E alpha), then add to initial temperature.

# Source Slide Checklist

This is a compact OCR/text extraction from the source PDF. Use it as a searchable reminder of the slide wording, not as a replacement for diagrams.

## Source page 1

THERMAL PROPERTIES

OF MATERIALS

## Source page 2

THERMAL PROPERTIES: knowledge of materials response to the

application of heat.

The knowledge of materials behaviour at high temperatures and how

their properties change with temperature is fundamental for material

applications

MATERIAL

 Temperature rise

 Dimensions increase

 Energy transport to cooler regions

 Melting

HEAT

RELEVANT THERMAL PROPERTIES:

 Heat capacity

 Thermal conductivity

...

## Source page 3

Mechanisms of heat transfer in a solid material

If heat is supplied to a solid material:

 atomic vibrational energy

increases

 atoms are not independent (

due to

their chemical bonds ): heat is

transferred through the material

(crystalline lattice or amorphous

structure) by vibrational waves called

PHONONS

Thermal energy is transferred:

- both by free electrons (for instance in metals , where there is an

“electronic cloud”)

...

## Source page 4

The modes of vibration involve the entire crystal

volume.

In real crystals, amplitude of vibration is typically

much smaller than the lattice spacing.

## Source page 5

5https://www.youtube.com/watch?v=RgRwHL4P8tU

## Source page 6

The internal energy of a solid material increases as heat is provided to it.

Thermal vibration amplitude increases as heat is supplied to the material

temperature increases  the kinetic energy of electrons increases and

the interatomic distance increases  the solid changes its size

Thermal vibrations:

 Atomic, ionic and molecular vibrations around the

equilibrium positions of an atom/ion/molecule in the lattice

 Atomic vibration inside molecules

 Rotation of molecules

During phase transformations (e.g. transitions of state of matter)

heat is spent to do the transformation

and there is no temperature increase

## Source page 7

The heat capacity , C (J/K), of a system is the ratio

between the heat added to a material (dQ) and the

resultant change in its temperature (dT):

Practically, it is the ratio between the absorbed

thermal energy ΔE and the resultant increase in

temperature ΔT:

HEAT MATERIAL

Heat capacity

This parameter denotes the material ability to absorb heat from the external

surroundings.

dT

dQC 

T

EC 

...

## Source page 8

To make a comparison of heat capacities of different materials, we introduce

a new parameter derived from C:

the SPECIFIC HEAT (c) represents the heat capacity per unit mass (i.e. 1

kg) to raise a material’s temperature by 1 degree (1 K)

 cp: measured with

constant external pressure

 cv: maintaining

specimen volume constant

cp > c v but the difference is

very small at room temperature, so we

can usually define a single value of

specific heat c.

dT m

dQc  (J/kg K)

...

## Source page 9

The heat capacity C (and accordingly the specific heat c) increases as T

increases (at relatively low temperature):

 it is necessary to give a bigger amount of heat to raise temper ature of a

former heated material

 above a certain temperature it becomes constant

DEBYE TEMPERATURE

(below room temperature for many solid materials)

## Source page 10

If the specific heat, c, is referred to 1 mole of substance (instead of 1 kg we

consider a number of atoms or molecules equal to the Avogadro ’s number,

NA = 6×10 32 ), it is called ATOMIC OR MOLECULAR HEAT (J/mole K). This

parameter is preferably used in chemistry and materials science.

For most of solid elements the ATOMIC HEAT is about 25 J/mol K.

 atomic heat depends on

temperature at low T

 at high T it is approximately

constant (or slightly over 25 J/mol

K)

Heat capacity and derived parameters

depend on the atomic weight.

## Source page 11

Thermal conductivity is the ability of a material to transfer thermal energy

from a system at high temperature to another system at lower temperature.

Thermal conductivity

HEAT

MATERIAL

We define the thermal power Q (W) as:

THERMAL CONDUCTIVITY

COEFFICIENT

1-D situation, e.g. in a wire

2 o m

W dx

dTkA

Qq  

Thermal flow

...

## Source page 12

Example

Calculate the heat flowed in 1 hour through a 2 mm thick polymeric sheet (1 m 2) when one

side is at 20 °C and the other side is at 50 °C.

k = 0.58 W/m K

Q = 1 × 0.58 × 30 / (2× 10 -3) = 8700 W

Heat in 1 h = 8700 × 3600 = 3.1 10 7 J

1 W=1 J / s

## Source page 13

Mechanisms of heat conduction

 Lattice vibration waves ( PHONONS )

 Free electrons

k = k l + k eTOTAL

CONDUCTIVITY

LATTICE VIBRATION

CONDUCTIVITY

Phonon net movement

ELECTRON

CONDUCTIVITY

Kinetic energy transfer

## Source page 14

First mechanism ( free electrons ) is predominant in metals : it is

related to electrical conductivity (also in this case we hav e movement

of electrons) and it is very efficient  metals have high thermal

conductivity . It can also depend on impurities and alloying elements.

Second mechanism ( phonons ) is predominant in ceramics and it is

less efficient  in fact ceramics are insulating materials

Thermal conductivity of glasses is lower than thermal conductivity

of ceramics  vibrational waves very hardly propagate without

crystalline lattice

Porous materials  low thermal conductivity (air entrapped inside

the pores is a bad heat conductor  desired thermal insultating effect )

Thermal conductivity of polymers is lower than thermal

conductivity of ceramics (heat is partially dissipated by

vibration/rotation of polymeric chain molecules); it is as much lower if

...

## Source page 15

In general, thermal conductivity depends

on temperature.

Random thermal agitation increases with increasing

temperature  disturbing effect on propagation of phonons

(for instance kl decreases with the increase of T in the

case of ceramics ).

Electrons motion does not change (significantly) with T

(practically, ke does not change with T in the case of

metals )

However, remember that BOTH MECHANISMS are always present

in solid materials!

## Source page 17

METALS

CERAMICS

In most cases, metals exhibit higher thermal conductivity than ceramics.

k metals > kceramics >> kpolymers

## Source page 18

Some practical effects of heat capacity and thermal conductivity

A component made by using a material with high specific heat t akes

more time (in other words, more heat ) to increase its temperature in

comparison with a component made of a material showing a low

specific heat.

Example:

Why is steel cold to touch?

Because steel has high thermal conductivity and high specif ic heat;

as a consequence, it is cold to the touch  heat flux from our body is

significant (high thermal conductivity) and a big amount of heat is

needed to raise steel’s temperature from room temperature ( 25 °C)

up to equilibrium with our hand (37 °C) (

steel has high heat capacity ).

## Source page 19

k vs Zn % in Cu-Zn alloys

## Source page 20

POLYMERS

k ~ 0.3 W/m K

Vibration and

rotation of

molecular chains

k increases with

the % of

crystalline

structure

Typical insulating

materials

Polymeric Foams:

role of pores

## Source page 21

Role of porosity on thermal

conductivity

•k (air) = 0.02 W/m K

Foam glass, k= 0.04 W/mK

Foam materials

## Source page 22

Silica aerogel

• One of the lowest density material

(1.6-1.9 mg/cm 3)

• 95% air, 5% SiO 2

• pore size about 20 nm

20 nm

## Source page 23

Thermal conductivity of Aerogels vs

other insulating materials

Air

## Source page 24

k aerogel < k air: is it possible?

Pore size in aerogel (20 nm) is lower than free mean

path for air molecules: heat transmission less effective in

aerogels than in air (convection)

## Source page 25

Atoms with similar mass

High E (diamond E=700-1200GPa)

Low defects

Simple crystalline cell (e.g. cubic)

Diamond 2000 (W .m-1. K-1)

Graphite anisotropic

 see next slide

BN (cubic) 1300

BeO 300

AlN 200

SiC 130

High-k ceramics

## Source page 26

Graphite: anisotropy

## Source page 27

Applications of high k ceramics: SiC heat exchangers

W.m-1. K-1

## Source page 28

Thermal conductivity in ceramics: the

influence of grain size

• Effect of grain size:

like in the case of mechanical resistance

(strength), the increase of thermal resistance,

k

-1, is related to the grain size d, being

inversely proportional to √d :

k -1  d -1/2

• For ceramics to have high thermal

conductivity, MICROSTRUCTURES with

LARGE GRAINS are useful to minimize the

effect of phononoic deviation by grain

boundaries and the effect of phases/impurity

...

## Source page 29

Thermal expansion

In general, solids increase their

size when heated and decrease

their size when cooled .

We heat the rod up to a temperature T > T0, and its length increases to L

L L 0 T

The rod is at a temperature T0 and has a length of L0.

We shall call the change in temperature:

T T - T0

and the corresponding change in length:

L L - L0

HEAT

## Source page 30

Tl

lT Tl

l l

t    

  

0 ) (

Due to temperature increase ΔT, solids undergo thermal deformation that can

be defined as:

Thermal expansion is reflected by an increase in the average

distance between the atoms with respect to their equilibrium positions

the increase of volume due to thermal expansion is due to the

increase of interatomic bond length

 is called THERMAL EXPANSION COEFFICIENT [K -1 or °C -1]: it indicates

how a material expands upon heating

...

## Source page 31

 = 10×10 -6 C-1 means that, starting from about

room temperature, at 1000 °C elongation is 1%

Note: actually,  Is not constant but (slightly) varies with T

Metals   5-25 10 -6 K-1

Ceramics   0.5-15 10 -6 K-1

Polimers   50-400 10 -6 K-1

## Source page 32

CTE and bond

strength

Lower 

Strongly

bonded

solids,

high E,

high melt T

## Source page 33

Melting temperature (K)

Relationship between α at 25 °C and

melting temperature. Metals having

high melting point tend to show less

expansion

Strong chemical bond: high elastic modulus , high melting

point , low thermal expansion coefficient

## Source page 34

CTE changes with the crystalline

structure

(example: Fe)

## Source page 35

Examples:

 to manufacture a metallic joint using polymer resins as joining

material, additives (glass fibers or ceramics) should be pu t in the polymer

with the aim of reducing its thermal expansion coefficient

 Fe/steel reinforcement in

concrete : coupling between concrete matrix

(“artificial ceramic”) and metal-

Material design and choice should take into account the thermal

expansion of materials that are put in contact

Careful attention should be devoted to materials in compone nts working at

high temperature, used as a coating or subjected to sudden te mperature

changes   mismatch should be reduced and appropriate “voids” might

be foreseen inside components in order to allow thermal expansion

Importance of  in materials choice

## Source page 36

CTE steel = 12 x 10 -6 °C -1

CTE granite= 8 x 10 -6 °C -1

CTE steel = 12 x 10 -6 °C -1

CTE granite= 8 x 10 -6 °C -1

## Source page 37

 = E   E  l /l o  E  T

 Ductile materials

 Brittle materials

Thermally induced stresses

Tl

l

T Tl

l l

t

t

 

 





...

## Source page 38

 Brass cylinder (E= 100 GPa,  y= 172 MPa,  = 20 x

10 -6 /K ), no thermal expansion allowed, which is

the maximum T it can reach without plastic

deformation? (room T= 20 °C)

Troom

Lroom

T

L

compressive  keeps L = 0   E(thermal )  E(T  Troom )

100 GPa 20 x 10 -6 /K

20 °CT= 106 °C172 MPa

Thermally induced stresses: example

 = E   E  l /l o  E  T

## Source page 39

 B <  A  B >  A

Joined materials with different thermal expansion

coefficients- Residual stresses during cooling

 If α B > α A, during cooling to room T, material

A is in compression mode

 If α B < α A , during cooling to room T, material

A is in tensile mode

RT RT

A

BB

A

## Source page 41

Stress at the interface between two solids

having different CTE

 = Stress at the interface between two solids having different CTE

E = Young modulus (M=metal, C=ceramic)

T = temperature (Tb -Ta =

T)

 = CTE (M=metal, C=ceramic)

## Source page 42

• flexural strength, f

• coefficient of thermal conductivity, k

• elastic modulus, E

• TEC, 



E

kTSR

f



 First approximation of temperature variation ( T) without

failure for a given material

Thermal shock resistance (TSR)

MPa

BEST (ideal) MATERIAL: high k and low 

...

## Source page 43

Materiali per l’Ingegneria

M.Ferraris

Al

Cu

Au

Fe

Ni

Ag

W

Steel

Stainless steel

brass

Silica glass

Soda-lime glass

...

## Source page 44

DUCTILE MATERIALS

(e.g. metals, polymers)

Thermal stresses can induce plastic

deformation (unavoidable)

BRITTLE MATERIALS

(e.g. ceramics, glasses)

Thermal stresses

often lead

to

fracture

Modification of material properties ( mainly ) by:

 changing chemical composition (e.g. adding other

oxides in glasses;

 fabrication of composites (second phases with

...

## Source page 45

THERMAL PROPERTY MEANING CORRELATION TO

MATERIAL

CHARACTERISTICS

THERMAL CAPACITY Material ability to

absorb heat from the

external surroundings

Depends on atomic weight

THERMAL

CONDUCTIVITY

Material ability to

transfer thermal energy

from a system at high

temperature to another

system at lower

...