Lecture 05 - Phase Diagrams

Source: `STM/Material(1)/05_phase diagrams_2025-2026.pdf; STM/Material(2)/Exercises5-7`

Purpose: open-note exam guide. It prioritizes answer structure, formulas, tutorial methods, and professor-style traps.

# Core Idea

Phase diagrams are equilibrium maps. They show which phases exist at a given composition and temperature, what the phase compositions are, and what relative amounts are present. The professor expects you to read the diagram, not memorize an isolated formula.

# Definitions

Component: element or chemical compound whose presence is necessary and sufficient to define the system.

Alloy: mixture of two or more elements with metallic properties.

Binary system: two components.

Phase: homogeneous part of a system with uniform chemical and physical characteristics.

Monophasic system: one phase. Biphasic system: two phases differing by state, composition, and/or crystal structure.

Microstructure and properties depend on composition, temperature, and pressure; in binary condensed diagrams pressure is normally treated as constant.

# How To Read Any Binary Diagram

1. Locate the alloy composition on the x-axis and the temperature on the y-axis.

2. Identify the field: one phase or two phases.

3. In a one-phase field, the phase composition equals the alloy composition and the relative amount is 100%.

4. In a two-phase field, draw a horizontal tie line. The intersections with the boundaries give the compositions of the two phases.

5. Apply the lever rule for relative amounts.

6. If requested, describe the microstructure: primary phase, eutectic mixture, pro-eutectoid phase, precipitates, etc.

# Gibbs Rule

General form: V = C - f + n.

For condensed binary diagrams at constant pressure: V = C - f + 1 = 3 - f.

One-phase field in binary diagram: f = 1, V = 2. Temperature and composition can vary.

Two-phase field: f = 2, V = 1. If temperature is fixed, phase compositions are fixed by the tie line.

Three phases in binary condensed system: f = 3, V = 0. This is invariant, such as eutectic/peritectic reactions at fixed T and compositions.

# Horizontal Rule and Lever Rule

Horizontal/tie-line rule: draw a horizontal line across the two-phase region at the temperature of interest. The left and right boundary compositions are the phase compositions.

Lever rule formula: for phases at C1 and C2 and alloy at C, fraction of phase at C1 = (C2 - C)/(C2 - C1), fraction of phase at C2 = (C - C1)/(C2 - C1).

Memory trick: amount of a phase is the opposite length of the tie line.

Always multiply by 100 for percentage.

# Diagram Families

Complete solubility in liquid and solid state: examples Cu-Ni or Ag-Au. There is a liquidus, solidus, L, solid solution, and L+solid region.

Complete solubility in liquid but no solubility in solid: eutectic diagram with L transforming into A+B or alpha+beta.

Partial solubility in solid: eutectic diagram with alpha, beta, alpha+beta, L+alpha, L+beta fields and solvus lines.

Peritectic: L + delta <-> gamma.

Congruent melting compound: compound melts to liquid of same composition.

Non-congruent melting compound: compound decomposes/transforms with liquid plus another phase.

# Microstructure Language

Primary phase: phase that forms before an invariant reaction.

Eutectic structure: fine mixture formed by L -> alpha + beta at eutectic temperature/composition.

Hypoeutectic vs hypereutectic: composition respectively below or above eutectic composition. Describe primary phase plus eutectic constituent.

During cooling below a solvus, phase compositions change along solvus curves and relative amounts change by lever rule.

# Tutorial Checklist

Exercises 5-7 repeatedly ask: determine phases, compositions, relative amounts, and draw/schematize microstructure.

For any point labeled at the beginning/end of a eutectic transformation, be precise: just before the reaction, liquid may still be present; just after it, the liquid has transformed into the eutectic mixture.

If the question asks "complete solubility" vs "partial/no solubility", do not invent extra phases. Use the region labels from the diagram family.

# Exam Traps

Do not use the alloy composition as phase composition in a two-phase field. Use the tie-line endpoints.

Do not apply lever rule in a single-phase field.

Do not say a phase diagram is a kinetic cooling curve. These diagrams are equilibrium diagrams and assume slow cooling.

Do not forget that phase diagrams have temperature on y-axis and composition wt.% on x-axis in this course.

# Source Slide Checklist

This is a compact OCR/text extraction from the source PDF. Use it as a searchable reminder of the slide wording, not as a replacement for diagrams.

## Source page 1

PHASE DIAGRAMS

## Source page 2

Some definitions…

Component: element or chemical compound whose presence is

necessary and sufficient to make a system.

Alloy: mixture of two or more elements having metallic properties.

Binary systems

 two components.

## Source page 3

Phase:

A phase is a homogeneous portion of a system with uniform

chemical and physical characteristics (therefore, both in terms of

structure and composition).

A single phase has the same behavior in all its parts when subjected

to physical or chemical stresses

A phase can consist of more than one chemical component (such as

water or metallic solid solutions in which some atoms (solutes) are

placed within the crystalline structure of te other (in interstit ial or

substitutional positions)

A chemical element or compound can exist as different phases

(liquid water, water vapor and ice, Feα, Feγ)

## Source page 4

MONOPHASIC SYSTEMS

W ATER liquid ICE solid W ATER vapour

OIL liquid Fe FCC solid

ONLY ONE PHASE

## Source page 5

Water

and oil

Water and

ice

Solid solution +

second phase

BIPHASIC SYSTEMS

They are made of TWO different phases that differ in terms of:

• Aggregation state (e,g. liquid vs. solid) and/or

• Composition and/or

• Crystalline structure

## Source page 6

Properties of materials depend on microstructure  it

depends on composition, T, p

Equilibrium diagrams or phase diagrams are graphical

representations of the various phases (microstructures) i n a

system depending on composition and temperature

All the phase diagrams have:

- T on the y-axis

- composition (wt.%) on the x-axis

## Source page 7

A phase diagram is:

a graph describing how many and which phases of a system are

present when the intensive parameters (pressure, temperature) of the

system itself vary.

Phase diagrams are valid when the thermodynamic equilibrium is

reached (slow cooling).

Phase diagrams can be obtained experimentally or by calculations.

In 1-component phase diagrams, we consider both T and p.

In binary phase diagrams, we consider only the condensed phases

(solid and liquid)  p is considered not significant (constant).

## Source page 8

Phase diagrams are very useful for different applications; for

example, thanks to them you can:

- Determine the number and type of phases as temperature and

composition vary;

- Calculate the relative quantities of the phases present at the

equilibrium;

- Determine the maximum solubility, in equilibrium conditions, of

one component in another;

- Know the melting temperature of the various phases;

- Determine the temperature at which phase transformations occur.

## Source page 9

Gibbs’ rule or phases rule

Gibbs’ rule (phases rule) establishes mathematically the relati onship

between the number of variables that can change (V), the number of

components (C), the number of phases (f) and the number of

physical parameters (p, T):

V = C - f + n

Since p = cost, then the Gibbs’ rule can be rewritten as:

V = C - f + 1

In binary systems C = 2, thus:

V = 3 - f

## Source page 12

Classification of phase diagrams

- Full solubility in the solid state

- No solubility in the solid state (eutectic)

- Partial solubility in the solid state (eutectic)

- Peritectic

- Presence of congruent/non-congruent melting

## Source page 13

Complete solubility in liquid

and solid state

e.g. Cu-Ni or Ag-Au.

V=C-f+n

Curve of liquidus

Curve of solidus

## Source page 14

How to read composition of phases

## Source page 15

How to read % of phases

## Source page 16

How to read the structure morphology

## Source page 18

Effect of solid solution strengthening on:

Tensile strength ( TS ) Ductility ( %EL )

Adapted from Fig. 9.6(a),

Callister & Rethwisch 8e.

Tensile Strength (MPa)

Composition, wt% Ni

Cu Ni

0 20 40 60 80 100 200

TS for

pure Ni

TS for pure Cu

Elongation (%EL)

...

## Source page 19

“Eutectic” (from Greek) = “eu”, which means something easy or

good, and “tactic”, which is the process of melting. So the general

meaning in Greek is something that melts in a good manner .

L  α + β L  A + B or

## Source page 20

Complete solubility in the liquid state, no

solubility in the solid state

## Source page 21

Complete solubility in the liquid state,

partial solubility in the solid state

## Source page 23

Formation of a compound with congruent melting

In this case: complete solubility in the liquid state, no solubility in the

solid state

## Source page 25

Formation of a compound with non-congruent melting

In this case: complete solubility in the liquid state, no solubility in the

solid state

## Source page 26

Peritectic

transformation

L + d  g

## Source page 34

Supero il limite di

solubilità:

Compare la seconda

fase β

## Source page 36

B E

X Z

l and m are just above and

below the euctectic T

A

D

## Source page 41

Eutectic structure (Pb-Sn)

## Source page 42

RAFFREDDAMENTO DI LEGHE EUTETTICHE 2

## Source page 43

RAFFREDDAMENTO DI LEGHE EUTETTICHE 3

## Source page 44

RAFFREDDAMENTO DI LEGHE EUTETTICHE 3

Abbassando la

Temperatura al di sotto

di T E le fasi restano alfa

e beta, ma cambiano di

composizione e in

rapporto quantitativo

seguendo le curve di

solvus

## Source page 45

RAFFREDDAMENTO DI LEGHE IPEREUTETTICHE

## Source page 46

RAFFREDDAMENTO DI LEGHE IPEREUTETTICHE 2

## Source page 47

RAFFREDDAMENTO DI LEGHE IPEREUTETTICHE 3