Lecture 06 - Phase Diagram Examples and Fe-C

Source: `STM/Material(1)/06_phase diagrams examples_2025-2026.pdf; STM/Material(2)/Exercises8-9`

Purpose: open-note exam guide. It prioritizes answer structure, formulas, tutorial methods, and professor-style traps.

# Fe-C Reference Diagram

Fe-C reference diagram

Keep these landmarks in your notes:

0.022 wt.% C: approximate maximum solubility of C in ferrite at the eutectoid temperature.

0.76 wt.% C: eutectoid composition.

727 C: eutectoid temperature.

2.14 wt.% C: approximate maximum solubility of C in austenite at the eutectic temperature.

4.30 wt.% C: eutectic composition.

6.70 wt.% C: cementite Fe3C composition.

# Steel Microstructures at Room Temperature

Hypo-eutectoid steel, C < 0.8% in the slides: ferrite and pearlite.

Eutectoid steel, C about 0.8%: pearlite.

Hyper-eutectoid steel, C > 0.8%: cementite and pearlite.

Pearlite is the eutectoid mixture of ferrite + cementite formed from austenite.

Coarse pearlite forms at higher isothermal transformation temperature because diffusion is easier. Fine pearlite forms at lower temperature because diffusion distance is shorter and lamellae are finer.

Spheroidite/globular pearlite forms by heating pearlitic steel just below eutectoid temperature for a long time, for example 700 C for 18-24 h. Driving force: reduce ferrite/cementite interfacial area. Result: easier plastic deformation.

# Fe-C Lever Rule Recipes

Hypo-eutectoid, C0 < 0.76:

Pro-eutectoid ferrite = (0.76 - C0)/(0.76 - 0.022).

Austenite just before eutectoid = (C0 - 0.022)/(0.76 - 0.022).

At room temperature, pearlite fraction equals the austenite fraction just before eutectoid.

Hyper-eutectoid, C0 > 0.76:

Pro-eutectoid cementite = (C0 - 0.76)/(6.70 - 0.76).

Austenite just before eutectoid = (6.70 - C0)/(6.70 - 0.76).

At room temperature, pearlite fraction equals the austenite fraction just before eutectoid.

Worked tutorial examples:

0.20% C steel: pro-eutectoid ferrite = 76%, pearlite = 24%.

1.20% C steel: pearlite = 92.5%, pro-eutectoid cementite = 7.4%.

# Peritectic Exercise Pattern

Peritectic reaction in Fe-C: L + delta -> gamma.

For low-carbon steels near the peritectic, identify whether the point is L, L+delta, L+gamma, delta+gamma, or gamma.

Use the horizontal rule for phase compositions, then lever rule for relative amounts.

Example for 0.34% C at a two-phase L+delta point: if C_delta = 0.05 and C_L = 0.40, delta = (0.40 - 0.34)/(0.40 - 0.05) = 17%, liquid = 83%.

Example for 0.13% C on the same tie line: delta = (0.40 - 0.13)/(0.40 - 0.05) = 77%, liquid = 23%.

# Martensite, Tempering, Bainite

Martensite is produced when austenite transforms without enough diffusion for equilibrium ferrite/cementite formation. It is a hard, brittle, supersaturated phase and is not read as an equilibrium field on the Fe-C phase diagram.

Tempering martensite decomposes martensite into ferrite plus fine cementite particles. Tempered martensite improves toughness relative to as-quenched martensite.

Bainite is another non-equilibrium transformation product, typically represented by time-temperature transformation thinking rather than an equilibrium Fe-C diagram.

Exam trap: phase diagrams show equilibrium phases. Martensite is not located as a stable phase field on the equilibrium Fe-Fe3C diagram.

# Al-Cu/Precipitation Example

The lecture examples include precipitation hardening. If solubility decreases on cooling, a supersaturated solid solution can precipitate fine particles.

More solute can give a higher density of precipitates, increasing strength when precipitates obstruct dislocation motion.

Overaging/coarsening lowers strengthening because precipitates become fewer/larger and easier for dislocations to bypass.

# Exam Traps

Pearlite is not a phase; it is a microconstituent made of ferrite + cementite.

Pro-eutectoid ferrite/cementite forms before the eutectoid reaction; pearlite forms from the remaining austenite during the eutectoid reaction.

Do not use 6.70 as if it were pure carbon; it is cementite Fe3C composition in wt.% C.

If asked at 400 C for pro-eutectoid cementite in a hyper-eutectoid steel, the amount of pro-eutectoid cementite is still calculated from the 727 C eutectoid tie line; below 727 C the remaining austenite has transformed to pearlite.

# Source Slide Checklist

This is a compact OCR/text extraction from the source PDF. Use it as a searchable reminder of the slide wording, not as a replacement for diagrams.

## Source page 1

Phase diagrams: examples

## Source page 3

A3

## Source page 4

Steel microstructure at room

temperature

• Hypo-eutectoidic

(C<0,8%): ferrite

and pearlite

• eutectoidic

(C=0,8%): pearlite

• Hyper-eutectoidic

(C>0,8%):

cementite and

pearlite

## Source page 5

Hypo-eutectoidic Hyper-eutectoidic

Tensile

strength

Yield

strength

Mechanical strength

wt% carbon

Mechanical

properties of

steel

vs.

microstructure

## Source page 6

Trattamenti termici per gli

acciai

Materiali per l’Ingegneria

M.Ferraris 6

Mechanical properties of steel vs. microstructure

## Source page 8

655 °C 600 °C 534 °C 487 °C

Microstructure of pearlite formed at different isothermal T:

If > T  coarse pearlite (> diffusion)

If < T  fine pearlite (< diffusion)

## Source page 9

If a steel with pearlitic microstructure is heated just below

eutectoidic T for long time (e.g. 700 °C 18-24 h)  globular

pearlite or spheroidite .

Driving force  minimizing the interfacial surface area

between ferrite and cementite.

## Source page 10

Spheroidite  < interfacial area  < density of GBs 

easier plastic deformation

## Source page 11

Martensite

Austenite  Martensite

Fast cooling from A3 to RT (quenching)

A3: point of austenitization (mobile point!)

Martensite: polymorphic transformation of austenite to

martensite (single phase)  it can host a higher amount of

C  solid solution effect against motion of dislocations.

## Source page 12

Microstructure and mechanical properties of steels

## Source page 13

Tempering

Increase of ductility and toughness of martensite  heat treatment at

250-650 °C

Phase transformation:

martensite  ferrite + cementite

Tempered martensite: fine particles of cementite in a matrix of ferrite

 sorbite (similar to spheroidite)

## Source page 14

For tempered martensite:

 > tempering T 

 > rate of particle

growth 

 residual ferrite with low

C 

 > ductility but < yield

strenght and hardness

## Source page 15

Heating to

complete

austenitization

Increase

dislocations….

quenching

## Source page 16

Leghe di allumino Materiali per l’Ingegneria

M.Ferraris 16

## Source page 17

Al-Cu

Precipitation hardening for Al-Cu alloys

CuAl 2

intermetallic

## Source page 18

a

Al-Cu

Precipitation hardening for Al-Cu alloys

## Source page 19

a

Al-Cu

Precipitation hardening for Al-Cu alloys

## Source page 20

• Example of

precipitation

hardening: Al-Cu, Cu-

Sn (bronze), Mg-Al,

….

o invecchiamento

## Source page 21

Here to maximize mechanical strength

Guinier-Preston zones

## Source page 23

Mechanical

properties vs.

microstructure of Al

alloys and thermal

treatments

Higher amount of Cu  higher reinforcing

effect  higher density of precipitates

## Source page 24

Practical examples of the use of

phase diagrams in materials design

## Source page 26

a b c

At 205 °C  (ab/ac)×100 = 65%

## Source page 27

P

## Source page 29

Historical example

In 1958, at the beginning of the US space project, an

engineer proposed to use tungsten (W) with a purity of

99.9% as the material for the exhaust nozzles of the

engines.

The choice was based on a few points:

• tungsten has a melting temperature of 3410 °C, about

400 °C above the temperature of the exhaust gases;

• tungsten is hard and can resist abrasion due to hot

exhaust gases

• tungsten was not too expensive ($ 25,000 per nozzle) as

compared to advanced ceramics at that time

## Source page 30

Three prototypes are produced and tests started.

The first nozzle only resisted a few seconds at about 3000

°C and then melted

The second and third nozzles melted even before reaching

3000 °C

The residues of the two destroyed nozzles were analyzed;

the composition of the material was, in both cases, W =

98.5% and C = 1.5%

## Source page 31

~ 0,1% C