Lecture 08 - Glass and Related Products

Source: `STM/Material(1)/08_glass 2025-2026.pdf`

Purpose: open-note exam guide. It prioritizes answer structure, formulas, tutorial methods, and professor-style traps.

# Core Idea

Glass is amorphous: no long-range atomic order, but short-range order exists. Silica glass keeps local SiO4 tetrahedra but lacks the ordered long-range quartz structure. Glasses do not have a sharp melting point like crystals; they progressively soften around the glass transition temperature Tg.

# Glass Transition and Formation

Crystalline solids have a melting temperature Tm. Glasses have a glass transition temperature Tg above which they progressively soften.

Tg can be viewed as the temperature where glass changes from rigid/brittle to rubber-like behavior. In many commercial glasses Tg is roughly 2/3 Tm.

Glass-forming liquids cool below solidification temperature without crystallization because viscosity becomes so high that random liquid structure is frozen in.

Glass is metastable; devitrification is crystallization of glass, which can occur over long times or be accelerated by thermal treatment below Tm.

Any substance that can turn into an amorphous state under suitable conditions can be called a glass: ceramics, amorphous metals, organic compounds, polymers, and some native elements.

# Glass vs Ceramics vs Glass-Ceramics

Fully crystalline ceramics: rocks/stones, cements, alumina, zirconia, etc.

Glasses: completely amorphous, non-crystalline ceramic sub-family.

Glass-ceramics: crystalline phases embedded in residual glass. They are made by deliberate devitrification of a parent glass to improve strength, hardness, stiffness, or thermal shock resistance.

# Glass Constituents and Composition

Network formers: oxides such as SiO2 and B2O3 that can form the glassy network.

Network modifiers: oxides such as Na2O and CaO that do not form the network alone but enter it and break bridging oxygens, producing non-bridging oxygens.

Intermediates: oxides such as Al2O3 and TiO2 that can enter/stabilize the network.

Soda-lime-silica glass (SiO2-Na2O-CaO) is low-cost, easy to process/form, stable in water, and used for windows, vehicle glass, windscreens, and light bulbs. Al2O3 increases durability.

# Glass Synthesis and Processing

Most common route: mix reagents in crucible, melt above 1000 C, then quench/form by pouring, pressing, blowing, or drawing into fibers.

Float glass production uses a molten tin bath to make flat glass sheets.

Colored glasses are obtained by adding chromophore ions as small amounts of metal oxides.

# Mechanical Behavior and Properties

Glasses are brittle and contain surface/macroscopic defects. Stress concentration near pores/cracks explains low tensile/flexural strength compared with compressive strength.

Typical common glass properties from slides: density around 2.5 g/cm3, Young modulus about 75 GPa, compressive strength about 1000 MPa, tensile/flexural strength about 40 MPa for common glasses and up to 200 MPa for special glasses, CTE about 9 x 10^-6 K^-1, very low thermal conductivity, refractive index about 1.5.

Fracture toughness relation: KIc = Y sigma_c sqrt(pi a). Strength depends on defect size, stress, and geometry.

# Safety Glass - Open Answer Block

Safety glass is a design response to the brittleness and defect sensitivity of glass. A complete answer should mention the loads and the safety mechanism.

Loads glass sheets can face:

Dynamic loads: wind, pressure of crowd.

Static loads: own weight, snow, hydrostatic pressure.

Accidental loads: hail, vibration, torsion, seismic phenomena.

Soft-body impact: people/animals.

Hard-body impact: stones or burglary tools.

Projectile impact: firearms.

Thermal shock: fire.

Armoured glass:

Contains a metallic network inside the glass.

Mechanical strength is only slightly improved, but in fire the network delays flame propagation and helps keep softened/broken glass in position.

Tempered glass:

Physical thermal tempering or chemical strengthening creates permanent compressive stress on the surface and tensile stress in the core.

Surface compression improves impact resistance because cracks must overcome compression before opening.

Chemical tempering can use ion exchange: larger K+ ions replace smaller Na+ ions near the surface, inducing compressive stress.

Multilayered/laminated glass:

Combines glass sheets with a polymeric interlayer.

It has good shock resistance, rupture is localized, and fragments remain attached to the polymer sheet instead of scattering.

# Foamed Glass

Foamed/cellular glass is used for thermal and acoustic insulation. It has a cellular, waterproof, gas-proof structure with many small closed, non-interconnected pores.

Main features: good insulation, low density, chemical stability, adequate compressive strength.

Air is a poor heat and sound conductor, so closed pores are useful.

Foam glass can be made from waste glass, broken windscreens, recycled glass, silica sandstone, and coal powder. Heating in molds around 600-800 C sinters glass powders and gas bubbles expand the mass.

# Static Fatigue and Stress Corrosion

Glass strength can decrease over time. A glass can break after a certain time under a static stress lower than expected.

This is static fatigue: defect population evolves with time.

In silica-based glasses/ceramics, water molecules attack deformed Si-O-Si bonds at crack tips. Stress plus chemical attack causes subcritical crack growth even when K < KIc.

Final reaction idea from slide: bridging oxygen removal interrupts the network and extends the crack.

# Exam Traps

Glass is amorphous but has short-range order.

Tg is not Tm. Glass softens progressively instead of melting sharply.

Tempering does not remove all tensile stress; it intentionally creates surface compression and core tension.

Armoured glass is mainly about holding the sheet in place/flame delay, not huge bending-strength improvement.

Foamed glass is for insulation, not transparent window panes.

# Source Slide Checklist

This is a compact OCR/text extraction from the source PDF. Use it as a searchable reminder of the slide wording, not as a replacement for diagrams.

## Source page 1

GLASS

and related products

## Source page 2

Glasses exhibit an AMORPHOUS STRUCTURE :

 they have a disordered structure (non-crystalline);

 there is no long-range atomic order;

 there is short-range atomic order.

Glass structure

SiO 2 Non-crystalline

(silica glass)

Crystalline

(quartz)

Note that in silica glass the short-range order is only represented by the [SiO 4]4-

tetrahedral unit (1 atom of Si surrounded by 4 atoms of O, forming a “pyramid”)

 Si atom

o O atom

## Source page 3

today/new-energy-landscapes-

reveal-glass-states-have-rough-

fractal-basins

Glass is a mystery.

That’s because glasses are amorphous and lack the

degree of order achieved in crystalline structures. In a

glass, molecules are held in place by their neighbor

molecules in less predictable and disordered

configurations.

Because of these interesting features, the

thermodynamics of glass states are not described by a

simple model. But research from Duke University offers

insights that may be help to unlock these mysteries by

providing a new

...

## Source page 4

Glass solidification Crystal solidification

Glasses do not solidify in the same sense of crystalline materials: u pon cooling,

glasses become more and more viscous and there is no definite temperature at

which the liquid transforms into solid as for crystalline materials.

GLASSES:

glass transition temperature T g

above which glass

progressively softens

Tg

CRYSTALLINE SOLIDS:

melting temperature T m

## Source page 5

Bonds in amorphous solids (e.g.

glasses) do not break all

together at a certain

temperature T

m: an exact

melting point cannot be defined,

but the amorphous solids

soften step by step .

Tg can be practically viewed as the temperature at which glass s tarts to

change from a rigid state to a “rubber-like state”.

In glasses, we can define T m as “liquid temperature”, i.e. the temperature

above which the material becomes a stable liquid (it complet ely changes

from a “rubber-like” state to a liquid state).

## Source page 6

Specific volume

temperature

glass

Crystalline material

liquid

Undercooled liquid

two options here !

Tg Tm

Glass: internal «friction»

among molecules!

## Source page 7

Glass transition temperature

1.7

Most commercial glasses are obtained by rapid cooling of a

viscous liquid below a typical “freezing” temperature, known as

glass transition temperature , Tg.

Such T is fundamental to define the properties of a certain

glass:

- It is in general around 2/3 of the melting T  Tg = 2/3 Tm

- above Tg the glass has a rubber-like behaviour

- below Tg the glass is a rigid and brittle material

## Source page 8

1. Ceramics: - inorganic oxides  traditional glasses (SiO 2, TeO 2, etc.)

- inorganic fluorides  fluoride glasses

- inorganic chalcogenides  chalcogenide glasses

2. Metals: amorphous metals (obtained by casting molten metal on thin

tapes with cooling speed of 10 7 °C/s)

3. Organic compounds: glycerin, glucose (caramel)

4. Polymers: in polymers amorphous zones are always present (PET),

some polymers are almost completely amorphous (e.g. PMMA)

5. Some native elements like S, Se, P

General definition of “glass” : any substance that, under suitable

conditions, can turn into the amorphous state

Types of amorphous materials

## Source page 9

Glass-forming liquids : upon cooling, viscous molten material (mixtures of

inorganic oxides such as SiO 2, CaO, Na 2O, MgO…) reaches a temperature

below the solidification temperature without crystalliza tion  there is no time

for crystalline structure formation during conventional c ooling of a glass-

forming liquid.

This occurs as atomic arrangement in liquid material

is blocked by high

viscosity : the random atomic structure of the liquid is “frozen” in the solid state

out of thermodynamic equilibrium.

Example : viscosity of SiO

2 fused at 1720 °C is about 10 8 times higher that

that of H2O at 20 °C!!!

Amorphous structures are thermodynamically metastable (they do not

represent the configuration at the lowest energy) ; therefore, they

...

## Source page 10

Note that glasses formally belong to the class of CERAMIC

MATERIALS .

In fact, we can divide ceramics into 3 sub-families:

 FULLY CRYSTALLINE CERAMICS (e.g. most of

rocks and stone

materials used in construction, that can be considered as “natural

ceramics”; cements , that can be considered “artificial ceramics”;

advanced or technical ceramics such as alumina and zirconia );

 GLASSES (completely amorphous, non-crystalline materials);

 GLASS-CERAMICS , in which one or more crystalline phases are

embedded in an amorphous matrix of residual glass; devitrification can

be deliberately carried out on starting glasses by thermal t reatment to

impart better properties to the material (for instance, gla ss-ceramics

exhibit superior mechanical properties, such as strength, hardness and

...

## Source page 11

NETWORK

FORMERS:

(e.g. SiO 2, B 2O3):

oxides able to form

glassy structure

NETWORK

MODIFIERS:

(e.g. CaO, Na 2O):

oxides that are not able

to form glassy

(polyhedral) networks

but their cations are

incorporated into the

glass network (e.g. in

...

## Source page 12

NETWORK FORMERS

NETWORK MODIFIERS

## Source page 13

+Na 2O

Glass structure: effect of alkali oxide

 Si ─ O ─ Si  + Na 2O →  Si ─ O -Na + + +Na -O ─ Si 

NBO: Non-Bridging Oxygen

BO: Bridging Oxygen

## Source page 14

Network of a

quaternary (4-oxide) glass

belonging to the

SiO 2-Al 2O3-NaO-CaO

system

## Source page 15

Pouring in moulds (e.g.

for windows) or in water

for very rapid cooling

Reagents mixing in a

crucible (e.g. SiO 2,

carbonates of Na and

Ca, Al 2O3…)

Melting in high-

temperature furnaces

(typically above 1000 °C)

Glass synthesis

The most commonly used method used for making glasses is the

melting-quenching route

Furthermore, upon cooling, soft glass can undergo pressing and/or air blowing (for

...

## Source page 16

Strain point < T g < Annealing point

Conventional

values of viscosity

## Source page 17

Float glass production  use of a melted TIN bath

## Source page 18

Coloured glasses

We can add chromophore ions in form of small quantities of special metal oxides

to the basic glass composition

## Source page 19

Mechanical behaviour of glasses

Usually glasses are not used as structural materials, but th ey can sustain

loads (windscreen and glass windows are exposed to wind, imp acts…)

Glasses are brittle materials!

Stress concentration near pores or

macroscopic defects (cracks, flaws)

 brittle materials show better

strength under compressive load

Mechanical properties of glasses, together with other

physical properties (e.g. optical properties, transparency…)

STRONGLY depend on GLASS COMPOSITION (= the type

and amount of the oxides we use for making the glasses)

## Source page 20

Density : 2.2-6.3 g/cm 3; for common glasses 2.5 g/cm 3

Hardness : 5.5-6.5 Mohs (for instance higher than metals, but lower than

quartz and granite)

Elastic (Young’s) modulus : E = 75 GPa

Compressive strength :  = 1000 MPa

Tensile/flexural strength :  = 40 MPa for common glasses; up to 200

MPa for special glasses

Thermal expansion coefficient: 9×10 -6 K-1 (lower than metals but quite

high: for instance, a 2-m long glass fiber shows elongation o f 0.72 mm

because of heating of 40 °C)

Thermal conductivity : very low

Thermal shock resistance : low for common glass, good for silica glass

Refractive index : n = 1.5 for common glasses

Typical features of glasses

## Source page 21

The most common glasses are silica-soda-lime (SiO 2-

Na 2O-CaO system) glasses:

 Low cost

 Easy processing and forming

 Good resistance to devitrification and stability in water

 Al 2O3 addition increases glass durability

 Uses: house windows, car/train windows, windscreens,

light bulb…

 Poor resistance to heat and to sudden changes of

temperature

## Source page 22

KIC critical

parameters

(defect length and

stress)

above which there is

failure ( all materials )

KIc = Y c (p a) 1/2

(ASTM E 399)

## Source page 23

Safety glasses

Designers must choose glasses taking into account some seve re

rules.

Glass sheets can be subjected to:

 Dynamic loads (wind, pressure of the crowd)

 Static loads (own weight, snow, hydrostatic pressure)

 Accidental loads (hail, vibrations, torsion, seismic phenomena)

 Impact with soft body (people and animals, usually accident al and

with low intensity)

 Impact with hard body (stones, burglary tools)

 Impact with projectile (fire-arms)

 Thermal shocks (fire)

## Source page 24

ARMOURED GLASS

Glass containing inside a metallic

network.

Mechanical strength is not particularly

enhanced (slight increase of bending

resistance) but there is

flame

propagation delay in case of fire 

if glass softens or breaks, metallic

network allows to maintain glass in its

position for certain period.

TEMPERED GLASS

Using physical (thermal  fast

solidification of the surface) or

...

## Source page 25

K+ ions are larger than

Na + ones and induce a

compressive state of

stress on the glass ion-

exchanged surface.

Chemically

tempered glass

## Source page 26

Float glass

Tempered glass

Multilayered glass

- Good shock resistance

- Rupture is localized

- Glass fragments remain attached to the

polymeric sheet

MULTILAYERED GLASS

## Source page 27

Foamed glass (or cellular glass)

Used for thermal and acoustic insulation, it has a cellular,

water-proof and gas-proof structure .

Main features: good insulation ability, low density, high chemical

stability, satisfactory mechanical performances (adequate

compressive strength).

It is characterized by a high amount of small, closed ( non-

interconnected ) PORES  suitable for thermal and acoustic

insulation (

air is a bad heat and sound conductor ).

It is used for civil building (load-bearing substructures for roof ,

paving, walls) and industrial use (high- or low-temperature

plants, gas tanks, chimneys, tunnels).

## Source page 28

cell

strut

Commercial name:

FOAMGLAS ®

Major constituents:

SiO 2 65.77 %wt.

Na 2O 13.44 %wt.

CaO 5.83 %wt.

Al

2O3 5.58 %wt.

Minor constituents:

Fe 2O3 , MnO, K 2O, SO 3,

BaO, TiO 2 , SrO, carbon

< 9.38 %wt.

...

## Source page 29

Attractive properties of FOAMGLAS ®: cheap, ease of

processing, eco-friendly

FOMAGLAS ® is an excellent material for civil construction and insulat ion

purposes. It is a lightweight, extremely fine-pored expand ed glass with

millions of hermetically sealed pores . Since no diffusion can take place,

the material is watertight and achieves an efficient barrie r against soil

humidity, vapour and aggressive agents from outside.

Besides the outstanding mechanical and thermal properties of the product,

foamed glass manufacture is an exemplary process for

WASTE

RECYCLING on an industrial basis. Foam glass can be manufactured fully

out of waste glass, with only a minimum of virgin additives.

Foamed is especially suitable for thin-walled thermal insu lations, such as

for

...

## Source page 30

Foamed glass is prepared by gas

blowing in a glass melt upon cooling,

or by introducing in the starting glass

composition particular components

that, upon heating (reagents melting)

can decompose developing gas .

Foamed glass processing is

eco-

friendly : the majority of the starting

raw material is constituted by glass

from broken windscreen, recycled

glass and silica sandstone.

Starting glass scraps are molten, and

the produced glass is ground and

...

## Source page 31

• FOAMGLAS ® is mainly fabricated in form of plates or panels (=

assembled plates), but can be also modelled in complex shapes.

• The plates and panels are normally put in place with the aid o f

molten bitumen (= blend of petroleum-derived natural

hydrocarbons) or by means of synthetic adhesives.

• FOAMGLAS ® is manually cut and requires no special tools for

installation or for the protection of the operator.

## Source page 32

Properties

and Uses of

Some

Glasses

and Glass-

Ceramics

Composition Property Use

Glasses

Al 2O3, MgO, CaO,

SiO 2

Translucent, chemicall

y

resistant

Window glass,

...

## Source page 33

Mechanical resistance of glass over time

The mechanical strength of glasses

and many ceramics tends to

progressively decrease over time

• After a certain time, glass breaks

due to a static stress which is lower

than the expected one.

• Thus: the defect population evolves

with time

This is a phenomenon known as

static fatigue .

## Source page 34

Effects of time need to be taken into account

Mech.

strenght

depends

on:

Stress-corrosion phenomena

(

static fatigue )

presence of defects  statistics

(e.g. Weibull)

Time-depending loads

(

dynamic fatigue )

## Source page 35

In glasses and silicon oxide-based

ceramics, water molecules break the

deformed bonds at the tip of the crack.

• There is an energy barrier to overcome

(threshold) in order to break the bonds

• Synergistic effects of stress and

chemical attack on bonds

• Crack propagation is limited by the

diffusion rate of the water (or aggressive

species) at the tip of the crack.

Crack tip

If the bridging oxygen (see crack tip) is removed  crack extension

Moist environment  crack propagation even if K < K IC

## Source page 36

Where the bridging oxygen Si-O-Si is removed, the glass netw ork is

interrupted (as it is interrupted along the crack)  corrosion and removal of

the bridging oxygen involves the extension of the crack (sub critical

propagation of crack).

If a load is applied that opens the crack 

accelerated propagation

-Si-O-Si- + (H +,OH -)water  -Si-OH + HO -Si-