Lecture 10 - Composite Materials

Source: `STM/Material(1)/10_composites 2025-2026.pdf`

Purpose: open-note exam guide. It prioritizes answer structure, formulas, tutorial methods, and professor-style traps.

# Core Idea

A composite is a combination of two or more chemically distinct and insoluble phases with a recognizable interface, arranged so properties/structural performance exceed the constituents acting independently. Usually one phase is a continuous matrix and another is reinforcement.

# Classification

By matrix: metal matrix composites (MMCs), ceramic matrix composites (CMCs), polymer matrix composites (PMCs/OMCs).

By reinforcement: fibers (long or short), particles, dispersions.

Reinforcement can be metal, polymer, ceramic, or glass depending on the composite design.

# Matrix and Bonding Logic

MMCs: matrix is relatively soft/flexible; reinforcement must have high strength/stiffness; reinforcement-matrix bond must be strong because load transfers from matrix to reinforcement.

PMCs: matrix is relatively soft/flexible; reinforcement must have high strength/stiffness; strong bond is needed for load transfer.

CMCs: matrix is hard and brittle; reinforcement should have high tensile strength to arrest crack growth; the reinforcement-matrix bond should be relatively weak enough to allow pull-out and crack energy dissipation rather than immediate brittle failure.

# Fiber-Reinforced Polymer-Matrix Composites

Fibers improve strength, fatigue resistance, Young modulus, and strength-to-weight ratio.

The fiber provides strength and stiffness.

The matrix binds fibers, transfers load between fibers, and protects them.

Common PMC fibers: glass fibers, carbon fibers, aramid fibers.

Common MMC fibers: boron, carbon, oxide ceramic, non-oxide ceramic fibers.

# Reinforcement Mechanisms

Fiber mechanisms: load transfer, debonding, pull-out, crack bridging/arrest.

Particle mechanisms: crack deviation, crack blocking, increased crack path, particle breaking, and energy consumption.

The useful mechanism depends on interface strength. A very strong interface is good for stiffness/load transfer in MMC/PMC; a controlled weaker interface can improve toughness in CMCs.

# Rule of Mixtures

The rule of mixtures predicts properties such as density, elastic modulus, electrical conductivity, and thermal conductivity from constituent properties and volume fractions.

Density: rho_c = rho_f f_f + rho_m f_m, with f_m = 1 - f_f.

Longitudinal modulus for continuous unidirectional fibers parallel to load: E_c = E_f f_f + E_m f_m.

Transverse modulus approximation: 1/E_c = f_f/E_f + f_m/E_m.

Trap: the high parallel modulus only applies when continuous fibers are aligned with the load.

# Processing

Pultrusion: resin-impregnated glass strands are pulled through a die, similar in idea to extrusion, producing pipes, channels, I-beams, etc.

Resin transfer molding: reinforcement preform is placed in a closed mold; thermoset matrix is injected; after curing, the part is ejected.

# Exam Traps

A composite is not just a mixture: phases must be distinct/insoluble with an interface and improved combined performance.

Matrix and reinforcement roles are different. Matrix is not necessarily the strongest phase.

In CMCs, a relatively weak interface can be beneficial for pull-out and crack arrest; do not apply the PMC/MMC strong-interface rule blindly.

Rule of mixtures must use volume fractions, not weight fractions, unless converted.

# Source Slide Checklist

This is a compact OCR/text extraction from the source PDF. Use it as a searchable reminder of the slide wording, not as a replacement for diagrams.

## Source page 1

COMPOSITE MATERIALS

## Source page 2

Some definitions

A composite material is a combination of two or more chemically distinct and

insoluble phases with recognizable interface, in such mann er that its

properties and structural performance are superior to thos e of the

constituents acting independently.

Generally, one material forms a continuous matrix while the other provides

the reinforcement.

Composites can be classified by their matrix material which include:

- Metal matrix composites (MMCs)

- Ceramic matrix composites (CMCs)

- Polymer matrix composites (PMCs) or sometimes referred to as

organic matrix composites (OMCs)

## Source page 4

MMCs - Metal Matrix Composites

- The matrix is relatively soft and flexible.

- The reinforcement must have high strength and stiffness

- Since the load must be transferred from the matrix to the reinforcement, the

reinforcement-matrix bond must be strong.

MMCs use:

-Two types of particulates (dispersion strengthened alloy s and regular

particulate composites)

- Or long fiber reinforcements

PMCs - Polymer Matrix Composites

- The matrix is relatively soft and flexible

- The reinforcement must have high strength and stiffness

- Since the load must be transferred from matrix to reinforce ment, the

reinforcement-matrix bond must be strong

CMCs - Ceramic Matrix Composites

- The matrix is relatively hard and brittle

- The reinforcement must have high tensile strength to arrest crack growth

- The reinforcement must be free to pull out as a crack extends , so the

...

## Source page 7

Load trasfer

Debonding (pull-out)

Reinforcement mechanisms due to fibres

## Source page 11

- Fiber reinforced composites provide improved strength, f atigue resistance,

Young’s modulus and strength to weight ratio over the constituent materials.

- This is achieved by incorporating strong, stiff, yet britt le fibers into a more

ductile matrix.

- Generally speaking the fiber supplies the strength and sti ffness while the

matrix binds the fibers together and provides a means of tran sferring the load

between fibers

- The matrix also provides protection for the fibers

Fiber-reinforced polymer-matrix composites

## Source page 13

The rule of mixtures predicts some properties of the composite (e.g. density,

elastic modulus, electrical conductivity, thermal conductivity) knowing

the properties and volume fractions ( f) of matrix and reinforcement.

f f m m cf f





 

Where the subscripts m and f refer to the matrix and fiber.

f mf f1 that Note

Rule of mixtures

The rule of mixtures can also be used to predict the modulus of elasticity

when the fibers are continuous and unidirectional.

Parallel to the fibers, the modulus of elasticity may be as high as:

f f m m cE f E f E

m

m

f

f

...

## Source page 16

Some commonly used fibers for

polymer matrix composites:

- Glass fibers

- Carbon fibers

- Aramid fibers

Some commonly used fibers for metal

matrix composites:

- Boron fibers

- Carbon fibers

- Oxide ceramic and non-oxide

ceramic fibers

## Source page 18

PULTRUSION

- Similar to extrusion of metallic parts

- Pultrusion involves pulling resin-impregnated glass strands through a die

- Standard extruded shapes can easily be produced such as pip es, channels,

I-beams, etc.

## Source page 19

RESIN TRANSFER MOLDING

- Resin transfer molding is a manufacturing method that is qu ite similar to

injection molding where plastic is injected into a closed mold

- In the RTM process the preform (precut piece(s) of reinforc ement) is placed

in the mold, the mold is closed and the thermoset plastic matr ix is injected into

the mold, once the matrix is cured the part is ejected

## Source page 20

DEVIATION

BLOCKING

INCREMENT OF

CRACK PATH

PARTICLE

BREAKING

Energy

consumption

Reinforcement mechanisms due to particles